info@persis-intl.com

| JIS G2201 Pig iron for steel making |  |  |  |
| --- | --- | --- | --- |
| JIS G2202 Foundry pig iron |  |  |  |
| JIS G2301 | Ferromanganse | ASTM A99-82 | Spec. for ferromanganese |
| JIS G2302 | Ferrosilicon | ASTM A100-80 | Spec. for ferrosilicon |
| JIS G2303 Ferrochromium ASTM A101-80 |  |  | Spec. for ferrochromium |
| JIS G2304 Silicon- ASTM A483-64 manganese |  |  | Spec. for silicon-manganese |
| JIS G2306 | Ferrotungsten | ASTM A144-73 | Spec. for ferrotungsten |
| JIS G2307 | Ferromolybdenum | ASTM A 132-89 | Spec. for ferromolybdenum |
| JIS G2308 Ferrovanadium ASTM A 102-92 |  |  | Spec. for ferrovanadium |
| JIS G2309 Ferrotitanium ASTM A324-73 |  |  | Spec. for ferrotitanium |
| JIS G2310 Ferrophosphorus |  |  |  |
| JIS G2311 Manganese metal ASTM A601-69 |  |  | Spec. for electrolytic manganese metal |
| JIS G2312 | Silicon metal |  |  |
| JIS G2313 | Chromium metal | ASTM A481-73 | Spec. for chrome metal |
| JIS G2314 Calcium silicon ASTM A495-76 |  |  | Spec. for calcium-silicon and calcium manganese-silicon |
| JIS G2315 Silicon-chromium ASTM A482-76 |  |  | Spec. for ferrochrome-silicon |
| JIS G2316 | Ferronickel |  |  |
| JIS G2318 | Ferroboron | ASTM A323-76 | Spec. for ferroboron |
| JIS G2319 Ferroniobium ASTM A550-78 |  |  | Spec. for ferrocolumbium |
| Bars, Shapes and Steel Plates |  |  |  |
| JIS G3101 Rolled steel for ASTM A36/ general structure A 36 M-91 |  |  | Spec. for structural steel |
| JIS G3106 Rolled steel for ASTM A 283/ welded structure A 283 M-92 |  |  | Spec. for low and intermediate tensile strength carbon steel plates of structural quality |
| ASTM A 284/ A 284 M-90 |  |  | Spec. for low and intermediate tensile strength carbon silicon steel plates for machine parts and general construction |
| ASTM A 529/ A529 M-89 |  |  | Spec. for structural steel with 42 ksi (290 MPa) Minimum yield point (1/2in. (12.7mm) Maximum thickness) |
| ASTM A 570/ A 570 M-92 |  |  | Spec. for hot rolled carbon steel sheet and strip, structural quality |
| ASTM A 572/ A 572 M-92a |  |  | Spec. for high-strength low-alloy columbium-vanadium steels of structural quality |
| ASTM A 573/ A 573 M-90 |  |  | Spec. for structural carbon steel plates of improved toughness |
| ASTM A633/ A 633 M-90a |  |  | Spec. for normalized high-strength low-alloy structural steel |
| ASTM A678/ A 678 M-92 ASTM A 709-92 |  |  | Spec. for quenched and tempered carbon steel plates for structural applications Spec. for structural steel for bridges |
| BS4360-90 |  |  | Spec. for weldable structural steels |
| BS EN 10025-90 DIN EN 10025-91 NF EN 10025-90 |  |  | Hot-rolled products of non-alloy structural steels-Technical delivery conditions |
| BS4360-86 (obsolete) |  |  | Weldable structural steels |
| DIN 17100-80 (obsolete) |  |  | Steels for general structural purposes |
| DIN 17102-83 |  |  | Weldable fine grain steels, normalized strip, plate, universal plate, sections and merchant |
| NF A 35-501-87(obsolete) |  |  | Structural steels. Grades and types. Sheets, medium and heavy plates, universal plates, bars and sections |
| ISO 630-80 |  |  | Structural steels |
| ISO 4950/2-81 |  |  | High yield strength flat steel products Part 2: Products supplied in the normalized or controlled rolled condition |
| ISO 4950/3-81 ISO 4951-79 |  |  | High yield strength flat steel product Part 3: Products supplied in the heat-treated (quenched + tempered) condition High yield strength steel bars and sections |
| ISO 4995-91 |  |  | Hot-rolled steel sheet of structural quality |
|  | ISO 4996-91 |  | Hot-rolled steel sheet of high yield stress structural quality |
| ISO 6316-82 |  |  | Hot-rolled steel strip of structural quality |

info@persis-intl.com

| JIS G 3128 | High yield strength ASTM A 514/ steel plates for A 514 M-91 welded structure |  | Spec. for high-yield strength, quenched and tempered alloy steel plate, suitable for welding |
| --- | --- | --- | --- |
|  | ASTM A 517/ A 517 M-90 |  | Spec. for pressure vessel plates, alloy steel, high-strength, quenched and tempered |
|  | ASTM A 709-92 |  | Spec. for structural steel for bridges |
|  | ISO 9328/4-91 |  | Steel plates and strips for pressure purposes - Technical delivery conditions - Part 4: Weldable fine grain steels with high proof stress supplied in the normalized of quenched and tempered condition |
| JIS G 3114 | Hot-rolled atmospheric ASTM A-588/ corrosion resisting A 588 M-91a steel for welded structure ASTM A709-92 |  | Spec. for high-strength low-alloy structural steel with 50,000 psi minimum yield point to 4 in. thick Spec. for structural steel for bridges. |
|  |  | BS EN10155-93 | Structural steels with improved atmospheric corrosion resistance |
|  |  | DIN EN10155-93 |  |
|  |  | BS4360-90 (Obsolete) | Weldable structural steels |
|  |  | VDEh 087-81 | Atmospheric corrosion resistance structural steels |
| NF A 35-502-84 |  |  | Structural steels with improved atmospheric corrosion resistance - Sheets, medium and heavy plates, universal plates, bars and sections |
|  | ISO 4952-81 |  | Structural steels with improved atmospheric corrosion resistance |
|  | ISO 5952-83 |  | Hot rolled steel sheet of structural quality with improved atmospheric corrosion resistances |
| JIS G 3125 | Superior atmospheric ASTM A 242/ corrosion resisting A242 M-91a rolled steels |  | Spec. for high-strength low-alloy structural steel |
|  | BS4360-90 |  | Weldable structural steels |
|  | NF A 35-502-84 |  | Structural steels with improved atmospheric corrosion resistance - Sheets, medium and heavy plates, universal plates, bars and sections |
|  | ISO 4952-81 |  | Structural steels with improved atmospheric corrosion resistance |
|  | ISO 5952-83 |  | Continuously hot-rolled steel sheet of structural quality with improved atmospheric corrosion resistances |
| JIS G 3103 | Carbon steel and molybdenum alloy ASTM A 204/ steel plates for A204 M-90 boilers and other pressure vessels |  | Spec. for molybdenum alloy steel plates for pressure vessels |
| JIS G 3115 | Steel plates for pressure vessels ASTM A 285/ for intermediate A 285 M-90 temperature service |  | Spec. for low and intermediate tensile strength carbon-steel plates of flange and firebox qualities for pressure vessels |
| JIS G 3116 | Steel sheets, ASTM A 414/ plates and strip for A 414 M-91 gas cylinders |  | Spec. for carbon steel sheets for pressure vessels |
| JIS G 3118 | Carbon steel plates for pressure vessels for ASTM A 515/ intermediate and A 515 M-90 moderate temperature service |  | Spec. for carbon steel plates of intermediate tensile strength for pressure vessel for intermediate and higher temperature service |
|  | ASTM A 516/ A516 M-90 |  | Spec. for carbon steel plates for pressure vessels for moderate and lower temperature service |
|  | ASTM A 612/ A 612 M-90 |  | Spec. for pressure vessel plates, carbon steel, high strength, for moderate and lower temperature service |
|  | ASTM A662/ A 662 M-90 |  | Spec. for pressure vessel plates, carbon-manganese for moderate and lower temperature service |
|  | BS EN 10028-2-93 DIN EN 10028-2-93 NF EN 10028-2-92 |  | Non-alloy and alloy steels with specified elevated temperature properties |
|  | BS EN 10028-3-93 DIN EN 10028-3-93 NF EN 10028-3-92 |  | Weldable fine grain steels, normalized |

info@persis-intl.com

Standard No.

Definition

Standard No.

Definition

| BS 1501/1-80 (Obsolete) |  | Steel for fired and unfired pressure vessels, plates |
| --- | --- | --- |
| DIN 17155-83 (Obsolete) |  | Boiler plate |
| NFA 36-205-82 (Obsolete) |  | Iron and steel, Steel plates for boilers and pressure vessels. Carbon and carbon manganese steel. Grades and types. |
| ISO 9328/2-91 |  | Steel plates and strips for pressure purposes - Technical delivery conditions - Part 2: Unalloyed and low-alloyed steels with specified room temperature and elevated temperature properties |
| ISO 9328/4-91 ISO 4978-83 |  | Steel pates and strips for pressure purposes - Technical delivery conditions - Part 4: Weldable fine grain steels with high proof stress supplied in the normalized or quenched and tempered condition Flat rolled steel products for welded gas cylinders |
| High strength |  |  |
| steel plates for |  |  |
| JIS G | pressure vessel for | Non-alloy and alloy steels with specified elevated temperature |
| 3124 | intermediate and BS EN 10028-2-93 | properties |
| moderate |  |  |
| temperature |  |  |
| service |  |  |
| DIN 17102-83 |  | Weldable fine grain steels, normalized strip, plate, universal plate, sections and merchant |
| BS 1501/2-88 (Obsolete) |  | Steels for pressure purposes: plate; spec. for alloy steels |
| ISO 9328/4-91 |  | Steel plates and strips for pressure purposes - Technical delivery conditions - Part 4: Weldable fine grain steels with high proof stress supplied in the normalized or quenched and tempered condition |
| Mn-Mo and Mn- |  |  |
| JIS G | Mo-Ni alloy steel ASTM A 302/ | Spec. for Mn-Mo and Mn-Mo-Ni alloy steel plates for pressure |
| 3119 | plates for boilers A 302 M-90 | vessels |
| and other pressure |  |  |
| vessels |  |  |
| Mn-Mo and Mn- |  |  |
| JIS G | Mo-Ni alloy steel ASTM A 533/ | Spec. for Mn-Mo and Mn-Mo-Ni alloy steel plates quenched and |
| 3120 | plates quenched A 533 M-90 | tempered for pressure vessels |
| and tempered for |  |  |
| pressure vessels |  |  |
| JIS G 4109 | Cr-Mo alloy steel ASTM A 734/ plates for pressure A 734 M-87a vessels | Spec. for pressure vessel plates, alloy steel and high strength low-alloy steel, quenched and tempered |
| ASTM A 387/ A 387 M-90a |  | Spec. for pressure vessel plates, alloy steels, chromium- molybdenum |
| BS EN 10028-2-93 DIN EN 10028-2-93 NF EN 10028-2-92 |  | Non-alloy and alloy steels with specified elevated temperature properties |
| BS 1501/2-70 (Obsolete) |  | Steels for pressure purposes: plate; spec. for alloy steels |
| DIN 17155-83 (Obsolete) |  | Boiler plates |
| NF A 36-206-83 (Obsolete) |  | Mo, Mn-Mo and Cr-Mo alloy steel plates for boilers and pressure vessels |
| ISO 9328/2-91 |  | Steel plates and strips for pressure purposes - Technical delivery conditions - Part 2: Unalloyed and low-alloyed steels with specified room temperature and elevated temperature properties |
| ISO 9328/3-91 |  | Steel plates and strips for pressure purposes - Technical delivery conditions - Part 3: Nickel-alloyed steels with specified low temperature properties |
| High strength |  |  |
| chromium- |  |  |
| molybdenum alloy ASTM A 542-91 |  | Pressure vessel plates, alloy steel, quenched and tempered, Cr- |
| JIS G | steel plates for | Mo and Cr-Mo-V-Ti-B Pressure vessel plates, alloy steel, Cr-Mo-V- |
| 4110 | pressure vessels ASTM A 832-91 | Ti-B |
| under high- |  |  |
| temperature |  |  |
| service |  |  |
| Carbon steel |  |  |
| JIS G3126 plates for pressure ASTM A 516/ |  | Spec. for pressure vessels, carbon steel, for moderate-and lower- |
| vessels for low A 516 M-90 |  | temperature service |
| temperature |  |  |

info@persis-intl.com

| service |  |  |  |
| --- | --- | --- | --- |
| ASTM A 537/ Spec. for pressure vessel plates, heat-treated, C-Mn-Si steel A 537 M-91 |  |  |  |
| ASTM A 662/ Spec. for carbon-manganese, pressure vessel plates, for A 662 M-90 moderate and lower temperature service |  |  |  |
| ASTM A 841/ A841 M-90 |  |  | Spec. for steel plates for pressure vessels, produced by the thermo-mechanical process |
|  |  | BS EN 10028-3-93 DIN EN 10028-3-93 NF EN 10028-3-92 | Weldable fine grain steels, normalized |
|  |  | BS 1501/1-80 (Obsolete) | Steels for pressure purposes: plates; spec. for carbon and carbon manganese steels |
|  |  | DIN 17102-83 | Weldable fine grain steels, normalized strip, plate, universal plate, sections and merchant bars |
|  |  | NF A 36-208-82 | Nickel alloy steel plates for low temperature boilers and pressure vessels |
|  |  | ISO 9328/4-91 | Steel plates and strips for pressure purposes - Technical delivery conditions - Part 4: Weldable fine grain steels with high proof stress supplied in the normalized or quenched and tempered condition |
|  | Nickel steel plates |  |  |
| JIS G 3127 | for pressure vessels for low temperature | ASTM A 203/ A 203 M-90 | Spec. for nickel alloy steel pressure vessel plates |
|  | service |  |  |
|  |  | ASTM A 353/ A 353 M-90 | Spec. for pressure vessel plates, alloy steel, 9% nickel, double- normalized and tempered |
|  |  | ASTM A 553/ A553 M-90 | Spec. for quenched and tempered 8 and 9% nickel and alloy steel pressure vessel plates |
|  |  | ASTM A 844/ A844 M-87b | Spec. for steel plates, 9% Nickel alloy, for pressure vessels, produced by the direct quenching process |
|  |  | BS 1501/2-88 (Obsolete) | Steels for pressure purposes: plates; spec. for alloy steels |
|  |  | DIN 17280-85 | Steel for use at low temperatures |
|  |  | NF A 36-208-82 | Nickel alloy steel plates for low temperature boilers and pressure vessels |
|  |  | ISO 9328/3-91 | Steel plates and strips for pressure purposes - Technical delivery conditions - Part 3: Nickel-alloyed steels with specified low temperature properties |
| JIS G 3104 | Steel bars for rivet | ASTM A 31-89 ASTM A 502-91 DIN 17111-80 | Spec. for boiler rivet steel and rivets Spec. for steel structural rivets Low carbon unalloyed steels for bolts, nuts and rivets |
| JIS G 3112 | Steel bars for concrete reinforcement | ASTM A 615-92b | Spec. for deformed billet-steel bars for concrete reinforcement |
|  |  | ASTM A 706/ A706 M-92b | Spec. for low-alloy steel deformed bars for concrete reinforcement |
|  |  | BS4449-88 | Hot-rolled steel bars for the reinforcement of concrete |
|  |  | DIN 488/1-84 | Reinforceing steels; grades, properties, marking |
|  |  | NF A 35-015-84 | Iron and steel product. Concrete reinforcing round bars |
|  |  | NF A 35-016-86 | Iron and steel product. Concrete reinforcing bars with improved adherence |
|  | Dimensions, | DIN 1013/1-76 | Steel bars; hot rolled rounds for general purposes, dimensions and tolerances |
|  | weight and |  |  |
| JIS G | permissible |  |  |
| 3191 | variations of hot |  |  |
|  | tolled steel bars |  |  |
|  | and bar in coil |  |  |
|  |  | DIN 1013/2-76 | Steel bars; hot rolled rounds for special purposes, dimensions and tolerances |
|  |  | DIN 1014/1-78 | Steel bars; hot rolled squares for general purposes, dimensions and tolerances |
|  |  | DIN 1014/2-78 | Steel bars; hot rolled squared for special purposes, dimensions and tolerances |
|  |  | DIN 1015-72 | Bar steel; hot-rolled hexagon steel, dimensions, permissible variations weights |
|  |  | DIN 59130-78 | Steel bars; hot-rolled rounds for bolts and rivets, dimensions, permissible variations, weights |

info@persis-intl.com

|  |  | NF A45-001-83 | General purpose rolled bars and sections - Rolling tolerances |
| --- | --- | --- | --- |
|  |  | NF A 45-003-79 | Hot rolled round steel bars - Dimensions |
|  |  | ISO 1035/1-80 | Hot rolled steel bars - Part 1: Dimensions of round bars |
|  |  | ISO 1035/4-82 | Hot-rolled steel bars - Part IV: tolerances of round, square and flat bars |
| JIS G 3192 | Dimensions, weight and permissible variations of hot- rolled steel sections | BS 4/1-80 | Structural steel sections; Hot-rolled sections |
|  | BS4848/4-72 |  | Equal and unequal angles |
|  |  | BS 4848/5-80 | Bulb flats |
| DIN 1019-77 |  |  | Bar steel; hot-rolled bulb plate; dimensions weight static properties, permissible deviations |
| DIN 1025/1-63 |  |  | Steel sections; hot-rolled narrow I-beams, I Range, dimensions, weights, static properties |
| DIN 1025/2-63 |  |  | Steel sections; hot-rolled wide I-beams (I-section wide flange beams), IPB Range and IB Range, dimensions, weights, static properties |
| DIN 1025/3-63 |  |  | Steel sections; hot-rolled I-beams, wide flange I-beams: light pattern, IPB1-series, dimensions, weights, tolerances, static values |
| DIN 1025/4-63 |  |  | Steel sections; hot-rolled I-beams: wide flange I-beams, heavy pattern, IPBv-series, dimensions, weights, tolerances, static values |
| DIN 1025/5-65 |  |  | Steel sections; hot-rolled I-beams: medium-flange I-beams, IPE- series, dimensions, weights, tolerances, static values |
| DIN 1026-63 |  |  | Bars, steel sections; hot-rolled rounded-edge channels, dimensions, weights, static properties |
| DIN 1028-76 |  |  | Bar steel; hot-rolled rounded-edge equal angles, dimensions, weights, static properties |
| DIN 1029-78 |  |  | Bar steel; hot-rolled rounded-edge unequal angles, dimensions, weights, static properties |
| NF A45-010-79 |  |  | Hot rolled unequal angle steel sections with radiused corners - Dimensions |
|  |  | NF A45-011-83 | Hot rolled bulb plate - Dimensions and tolerances |
|  |  | NF A45-209-83 | IPN beams - Dimensions |
|  |  | NF A45-210-83 | Standard beams and standard channel sections - Rolling tolerances |
|  |  | ISO 657/1-89 | Dimensions of hot-rolled steel sections - Part I: Equal-leg angles - Metric series - Dimensions and sectional properties |
|  |  | ISO 657/2-89 | Dimensions of hot-rolled steel sections - Part II: Unequal-leg angles - Metric series – Dimensions and sectional properties |
|  |  | ISO 657/5-76 | Hot-rolled steel sections - Part V: Equal-leg angles and unequal- leg angles - Tolerances for metric and inch series |
|  |  | ISO 657/11-80 | Hot-rolled steel sections - Part II: Sloping flange channel sections (Metric series) – Dimensions and sectional properties |
|  |  | ISO 657/13-81 | Hot-rolled steel sections - Part 13: Tolerances on sloping flange beam, column and channel sections |
|  |  | ISO 657/15-80 | Hot-rolled steel sections - Part 15: Sloping flange beam section (Metric series) - Dimensions and sectional properties |
|  |  | ISO 657/18-80 | Hot-rolled steel sections - Part 18: L sections for shipbuilding (Metric series) - Dimensions, sectional properties and tolerances |
|  |  | ISO 657/19-80 | Hot-rolled steel sections - Part 19: Bulb flats (Metric series) - Dimensions, sectional properties and tolerances |
| JIS G 3193 | Dimensions, weight and permissible variations of hot rolled steel plates, sheets and strip | BS EN 10029-91 | Spec. for tolerances on dimensions, shape and mass for hot rolled steel plates 3 mm thick or above |
|  |  | DIN EN 10029-91 | Spec. for tolerances on dimensions, shape and mass for hot rolled steel plates 3 mm thick or above |
|  |  | DIN 1543-81 (Obsolete) | Flat products of steel; hot rolled plates with thickness of 3 to 150 mm; tolerances on dimensions, mass and shape |
|  |  | ISO 7452-84 | Hot-rolled structural steel plates - Tolerances on dimensions and shape |

info@persis-intl.com

|  |  | NF EN 10029-91 | Spec. for tolerances on dimensions, shape and mass for hot rolled steel plates 3 mm thick or above |
| --- | --- | --- | --- |
|  |  | NF A 46-503-83 (Obsolete) | Iron and steel - medium and heavy plates - Tolerances on dimensions and excess weight |
| JIS G 3194 | Dimensions, weight and permissible variations of hot rolled steel flats | DIN 1017/1-67 | Bar steel; hot-rolled flat steel for general use, dimensions, permissible variations, weights |
|  |  | DIN 1017/2-64 | Bar steel; hot-rolled flat steel for special purposes (in bar drawing mills, bolt and screw factories, etc.) dimensions, permissible deviations, weights |
|  | NF A 45-005-80 |  | Hot rolled flat steel bars for general use - Dimensions |
|  |  | ISO 1035/3-80 | Hot-rolled steel bars - Part 3: Dimensions of flat bars |
| JIS G 3199 | Specification for through-thickness characteristics of steel plate and wide flat | ASTM A770-86 | Spec. for through-thickness tension testing of steel plates for special applications |
|  |  | BS 6780-86 VDEh SEL 096-88 | Spec. for through thickness reduction of area of steel plates and wide flats Steel flat products, sections, bars |
|  |  | DIN 50180-89 | Steel tensile test pieces taken perpendicular to the product surface to be used to determine the reduction of area |
|  |  | NF A 36-202-81 | Plates and wide flats with guaranteed properties in the direction perpendicular to the surface |
|  |  | ISO 7778-83 | Steel plate with specified through-thickness characteristics |
| JIS G 3350 | Light gauge steels for general structure | SSC 400 | Cold rolled steel sections |
|  |  | DIN 17118-76 | Cold rolled steel sections: technical condition of delivery |
|  |  | DIN 59413-76 | Cold rolled steel sections |
|  |  | NF A 37-101-77 | Steel cold formed sections, for common purposes |
| JIS G 3353 | Welded light gauge H steels for general structures | ASTM A 769/ A 769 M-90 | Spec. for electric resistance welded steel shapes |
| JIS A 5528 | Hot rolled steel sheet piles | ASTM A 328/ A 328 M-90 | Spec. for steel sheet piling |
|  |  | NF A 35-520-87 | Pile driving sections |
|  |  | NF A 45-020-90 | Larssen type pile driven sections |
| JIS E Rails 1101 Steel Plates and Sheets |  | ASTM A 1-84 BS 11-85 ISO 5003-80 | Spec. for carbon steel tee rails Spec. for railway rails Flat bottom railway rails and special rail sections for switches and crossings of not-treated steel - Technical delivery requirements |
| JIS G 3131 | Hot-rolled mild steel plate, sheet and strip | ASTM A 569/ A 569 M-91 | Spec. for steel carbon (0.15 maximum percent) hot-rolled sheet and strip, commercial quality |
|  |  | ASTM A 621/ A 621 M-91 | Spec. for steel sheet and strip, carbon, hot-rolled, drawing quality |
|  |  | ASTM A 622/ A 622 M-91 | Spec. for steel sheet and strip, carbon, hot-rolled, drawing quality, special killed |
|  |  | BS 1449/1 | Carbon and carbon-manganese plate, sheet and strip |
|  |  | SEC 1.2:91 | Spec. for hot rolled steel plate, sheet and wide strip based on formability |
|  |  | 1.4:91 1.8:91 | Spec. for hot rolled wide material based on specified minimum strength Spec. for hot rolled narrow strip based on formability |
|  |  | 1.10:91 | Spec. for hot rolled narrow strip based on specified minimum strength |
|  |  | 1.14:91 | Spec. for hot-rolled narrow strip supplied in a range of conditions for heat treatment and general engineering purpose |
|  |  | BS EN 10051:92 | Continuously hot-rolled uncoated plate, sheet and strip of non- alloy and alloy steels |
| DIN 1614/1-86 Flat products of steel; Hot-rolled strip and sheet of mild unalloyed steels; quality specifications |  |  |  |

info@persis-intl.com

|  |  | DIN 1016-87 | Hot rolled strip and sheet |
| --- | --- | --- | --- |
|  |  | DIN EN 10051 : 92 | Continuously hot-rollet uncoated plate, sheet and strip of non- alloy and alloy steels |
|  | NF A 36-102-87 |  | Hot rolled non alloyed mild steel strip for processing |
|  |  | NF A 36-301-92 | Continuous hot rolled strips. Plates and coils |
| NF EN 10051 : 92 |  |  | Continuously hot-rolled uncoated plate, sheet and strip of non- alloy and alloy steels |
|  |  | ISO 3573-86 | Hot-rolled carbon steel sheet of commercial and drawing qualities |
|  |  | ISO 6317-82 | Hot-rolled carbon steel strip of commercial and drawing qualities |
| JIS G 3141 | Cold rolled carbon steel sheets and strip | ASTM A109-91 | Spec. for cold-rolled carbon steel strip |
|  |  | ASTM A109 M-91 | Spec. for cold-rolled carbon steel strip (Metric series) |
|  |  | ASTM A366/ A366 M-91 | Spec. for steel, Carbon, cold-rolled sheet, commercial quality |
|  |  | ASTM A619/ A619 M-91 | Carbon steel sheet, cold-rolled, drawing quality |
|  |  | ASTM A 620/ A 620 M-91 | Carbon steel sheet, cold-rlled, drawing quality, special killed |
|  |  | BS 1449/1 | Carbon and Carbon-manganese plate, sheet and strip |
|  |  | SEC1.3 :91 | Spec. for cold rolled steel plate, sheet and wide strip for vitreous enameling based on formability. |
|  |  | 1.5: 91 1.9: 91 | Spec. for cold rolled wide material based on specified minimum strength Spec. for cold rolled narrow strip based on formability |
|  |  | 1.11:91 | Spec. for cold rolled narrow strip based on specified minimum strength |
|  |  | 11.15:91 | Spec. for cold rolled narrow strip supplied in a range of conditions for heat treatment and general engineering purposes |
|  |  | BS EN 10130:91 | Spec. for cold rolled low carbon steel flat products for cold forming |
|  |  | BS EN 10130:92 | Cold-rolled uncoated low carbon and high yield strength flat products for cold forming |
|  |  | DIN 1627-87 | Cold-rolled strip of soft unalloyed steels; quality specifications, in width not exceeding 650 mm |
|  |  | DIN EN 10130-91 | Spec. for cold rolled low carbon steel flat products for cold forming |
|  |  | DIN EN 10131:92 | Cold-rolled uncoated low carbon and high yield strength steel flat products for cold forming |
| JIS G3141 |  | DIN 1623/2-86 | Cold reduced sheet and strip: general purpose structural steels |
|  |  | DIN 1541-75 | Flat products of steel; cold-rolled wide mill strip and sheet of unalloyed steels; dimensions, tolerances on dimensions and form |
|  |  | DIN 1544-75 | Cold rolled steel strip: Dimensions, permissible variations on Dimensions and form |
|  |  | NF EN 10130-91 | Spec. for cold rolled low carbon steel flat products for cold forming |
|  |  | NF EN 10131-92 | Cold-rolled uncoated low carbon and high yield strength steel flat products for cold forming |
|  |  | ISO 3574-86 | Cold reduced carbon steel sheet of commercial and drawing qualities |
|  |  | ISO 5954-84 | Cold-reduced carbon steel sheet to hardness requirements |
|  | Decarburized steel |  |  |
| JIS G 3133 | sheets and strip for porcelain | ASTM A 424-91 | Spec. for steel for porcelain enamelling |
|  | enameling |  |  |
|  |  | ISO 5001-80 | Cold-reduced carbon steel sheet for vitreous enamelling |
|  |  | DIN 1623/3-87 | Steel flat products; cold reduced sheets and strip: mild unalloyed steels for vitreous enamelling |
| JIS G 3302 | Hot-dip zinc- coated steel sheets and coils | ASTM A361/ A361 M-85 | Spec. for steel sheets, zinc-coated (galvanized) by the hot-dip process for roofing |
|  |  | ASTM A446/ A446 M-91 | Spec. for steel sheet, zinc-coated by the hot-dip process, physical quality |
|  |  | ASTM A526/ A526 M-90 | Spec. for steel sheet, zinc-coated (galvanized) by the hot-dip process, commercial quality |

info@persis-intl.com

|  |  | ASTM A527/ A527 M-90 | Spec. for steel sheet, zinc-coated (galvanized) by the hot-dip process, lock-forming quality |
| --- | --- | --- | --- |
|  |  | ASTM A528/ A528 M-90 | Spec. for steel sheet, zinc-coated (galvanized) by the hot-dip process, drawing quality |
|  |  | ASTM A642/ A642 M-90 | Spec. for steel sheet, zinc-coated (galvanized) by the hot-dip process, drawing quality, special killed |
|  |  | BS EN 10142-91 BS EN 10143-93 | Spec. for continuously hot-dip zinc coated low carbon steel sheet and strip for cold forming Continuously hot-dip metal coated steel sheet and strip |
|  |  | BS EN 10147-92 | Continuously hot-dip zinc coated structural steel sheet and strip |
|  |  | BS 3083-88 | Hot-dip zinc coated and hot-dip aluminium /zinc coated corrugated steel sheets for general purposes |
|  |  | DIN EN 10142-91 | Spec. for continuously hot-dip zinc coated low carbon steel sheet and strip for cold forming |
|  |  | DIN EN 10143-93 | Continuously hot-dip metal coated steel sheet and strip |
|  |  | DIN EN 10147-92 DIN 59231-53 | Spec. for continuously hot-dip zinc-coated structural steel sheet and strip Corrugated sheet, tile sheet, galvanized |
| DIN 59232-78 |  |  | Flat steel products, hot galvanized wide strip and sheet of mild unalloyed steels and general structural steels |
| NF EN 10142-92 |  |  | Spec. for continuously hot-dip zinc coated low carbon steel sheet and strip for cold forming |
|  |  | NF EN 10147-92 | Continuously hot-dip zinc coated structural steel sheet and strip |
|  |  | NF A36-322-78 | Continuous hot-dip zinc-coated steel plates with required minimum yield stress intended for cold forming |
|  |  | ISO 3575-76 | Continuous hot-dip zinc-coated carbon steel sheet of commercial, lock-forming and drawing qualities |
|  |  | ISO 4998-91 | Continuous hot-dip zinc-coated carbon steel sheet of structural quality |
|  | Hot-dip zinc-5% |  |  |
| JIS G 3317 | aluminum alloy- coated steel | ASTM 875/ A875 M-88 | Aluminum alloy metallic-coated by the hot-dip process |
|  | sheets and coils |  |  |
| JIS G 3312 | Prepainted hod-dip zinc-coated steel sheets and coils | ASTM A755/ A755 M-89 | Spec. for steel sheet zinc-coated (galvanized) by the hot-dip process and coil-coated for roofing and siding, general requirements |
|  | Prepainted hot-dip | ASTM A755/ A755 M-89 | Spec. for steel sheet, metallic coated by the hot-dip process and prepainted by the coil-coating process for exterior exposed building products. |
| JIS G 3318 | zinc-5% aluminium alloy- coated steel |  |  |
|  | sheets and coils |  |  |
| JIS G 3313 | Electrolytic zinc- coated steel sheet | ASTM 591/ A591 M-89 | Spec. for electrolytic zinc-coated cold-rolled steel sheet |
|  |  | NF A 36-160-79 | Iron and steel - Electrolytic zinc-coated plates-coating prescription |
|  |  | ISO 5002-82 | Hot rolled and cold-reduced electrolytic zinc-coated carbon steel sheet of commercial and drawing qualities |
| JIS G 3303 | Tinplate and Black-plate | ASTM A624-90 | Single-reduced electrolytic tinplate |
|  |  | ASTM A624 M-90 | Spec. for tin plate, single-reduced electrolytic (metric) |
|  |  | ASTM A625-85 | Single-reduced black plate |
|  |  | ASTM A625 M-85 | Spec. for tin mill products, black plate, single-reduced (Metric) |
|  |  | ASTM A626-90 | Spec. for tin mill products, electrolytic tin plate, double-reduced |
|  |  | ASTM A626 M-90 | Spec for tin mill products, electrolytic tin plate, double-reduced (Metric) |
|  |  | ASTM A650/ A 650 M-88 BS EN 10203-91 | Spec. for tin mill products, black plate, double-reduced Spec. for cold reduced electrolytic tinplate |
| BS EN 10205-92 |  |  | Cold reduced blackplate in coil form for the production of tinplate or electrolytic chronium/ chronium oxide coated steel |
|  |  | DIN EN 10203-91 | Spec. for cold reduced electrolytic tinplate |
|  |  | DIN EN 10205-92 NF EN 10203-91 | Spec. for cold reduced blackplate in coil form for the production of tinplate or electrolytic chromium/chromium oxide coated steel Spec. for cold reduced electrolytic tinplate |
|  |  | NF EN 10205-92 | Cold reduced blackplate in coil form for the production of tinplate or electrolytic chromium/chromium oxide coated steel |

info@persis-intl.com

| ISO 1111/1-83 |  |  | Single cold-reduced tinplate and single cold- reduced blackplate - Part I: Sheet |
| --- | --- | --- | --- |
| ISO 1111/2-83 |  |  | Single cold-reduced tinplate and single cold-reduced blackplate - Part II: Electrolytic tinplate coil and blackplate coil for subsequent cutting into sheet form |
|  |  | ISO 4977/1-84 | Double cold-reduced electrolytic tinplate - Part I: Sheet |
|  |  | ISO 4977/2-88 | Double cold-reduced electrolytic tinplate - Part 2: Coil for subsequent cutting into sheets |
|  |  | ISO 5950-91 | Cryolite, natural and artificial, and aluminum fluodide for industrial use - Determination of phosphorus content - Reduced molybdophsphate photometric method |
| JIS G 3314 | Hot-dip aluminum coated steel sheets | ASTM A463-88 | Spec. for cold-rolled, aluminum type I and type II, steel sheet |
|  |  | BS 6830:87 | Continuously hot-dip aluminum/zinc alloy coated cold rolled carbon steel flat products |
|  |  | ISO 5000-80 | Continuously hot-dip aluminum-silicon-coated cold-reduced carbon steel sheet of commercial and drawing qualities |
| JIS G 3315 | Chromium Plated Tin Free Steel | ASTM A657-87 | Spec. for tin mill products, black plates, electrolytic Cr-coated, single and double reduced |
|  |  | BS EN 10202-90 | Spec. for cold reduced electrolytic chromium/chromium oxide coated steel |
|  |  | DIN EN 10202-90 | Spec. for cold reduced electrolytic chromium/chromium oxide coated steel |
| Steel Pipes |  | NF EN 10202-89 | Spec. for cold reduced electrolytic chromium/chromium oxide coated steel |
| JIS G 3452 | Carbon steel pipes ASTM A53-90 b for ordinary piping |  | Spec. for pipe, steel, black and hot-dipped, zinc-coated welded and seamless |
|  |  | API 5L-92 | Spec. for line pipe |
|  |  | BS 1387-90 | Steel tubes and tubulars suitable for screwing to B.S. 21 pipe threads |
|  |  | DIN 1615-84 DIN 2440-78 | Welded circular tubes of non-alloy steel without special quality requirements Steel tubes medium weight type suitable for screwing |
|  |  | DIN 2441-78 | Steel tubes, heavy-weight suitable for screwing |
|  |  | ISO 65-81 | Steel tubes suitable for screwing in accordance with ISO 7 |
|  |  | ISO 559-91 | Welded or seamless steel tubes for water, sewage and gas |
| JIS G 3454 | Carbon steel pipe for pressure service | ASTM A 135-89 a | Spec. for electric-resistance-welded steel pipe |
|  |  | ASTM A 53-90 b API 5L-92 | Spec. for pipe, steel, black and hot-dipped, zinc-coated welded and seamless Spec. for line pipe |
| BS 3601-87 |  |  | Steel pipes and tubes for pressure purposes. Carbons steel: Ordinary duties |
| BS 3602/1-87 |  |  | Steel pipes and tubes for pressure purpose. Carbon steel: High duties |
| DIN 1626-84 |  |  | Welded circular tubes of non-alloy steel with special quality requirements |
| DIN 1629-84 |  |  | Seamless circular tubes of non-alloy steel with special quality requirements |
| DIN 2442-63 |  |  | Steel tubes of specified quality suitable for screwing, nominal pressure 1 to 100 kg/cm2 |
|  |  | DIN 2448-81 | Seamless steel tubes, dimensions and weights |
|  |  | ISO 2604/2-75 | Steel products for pressure purpose - quality requirements - Part II : Wrought seamless tubes |
|  |  | ISO 2604/3-75 | Steel products for pressure purpose - quality requirements - Part III: Electric resistance and induction - welded tubes |
|  |  | ISO 9329/I-89 | Seamless steel tubes for pressure purposes; Part I: Unalloyed steel with specified room temperature properties |
|  |  | ISO 9330/I-90 | Welded steel tubes for pressure purposes - Technical delivery conditions - Part 1: Unalloyed steel tubes with specified room temperature properties |
| JIS G 3455 | Carbon steel pipes for high pressure service | BS 778-66 | Steel pipes and joints for hydraulic purposes |

info@persis-intl.com

| DIN 1628-84 Welded circular tubes of non-alloy steels with very high quality requirements |  |  |  |
| --- | --- | --- | --- |
| DIN 1630-84 Seamless circular tubes of non-alloy steels with very high quality requirements |  |  |  |
| ISO 2604/2-75 Steel products for pressure purposes - quality requirement - Part II: Wrought seamless tubes |  |  |  |
| ISO 9329/I-89 Seamless steel tubes for pressure purposes; Part I: Unalloyed steel with specified room temperature properties |  |  |  |
| Carbon steel pipes JIS G for high- ASTM A 106-91 Spec. for seamless carbon-steel pipe for high-temperature 3456 temperature service service |  |  |  |
| DIN 17175-79 Seamless tubes of high-temperature steels; technical conditions of delivery |  |  |  |
| DIN 17177-79 Electrically resistance of induction welded steel tubes for elevated temperatures; technical terms of delivery |  |  |  |
| Steel pipes and tubes for pressure purposes; carbon and carbon BS 3602/1-87 manganese steel with specified elevated temperature properties - Part I ; Seamless, electric resistance welded and induction welded tubes |  |  |  |
| ISO 2604/2-75 Steel products for pressure purposes - quality requirements - Part II: Wrought seamless tubes |  |  |  |
| ISO 2604/3-75 Steel products for pressure purposes - quality requirements- Part III: Electric resistance and inductance - welded tubes |  |  |  |
| JIS G Arc welded carbon ASTM A 134-90 Spec. for electric-fusion (arc)-welded steel plate pipe (sizes in 16 3457 steel pipes in. and over) |  |  |  |
| ASTM A 139/ Spec. for electric fusion (arc)-welded steel pipe (NPS in 4 in. and A139 M-90 over) |  |  |  |
|  |  | ASTM A 211-75 | Spec. for spiral-welded steel or iron pipe |
| DIN 1626-84 |  |  | Welded circular tubes of non-alloy steels with special quality requirements |
| ISO 559-91 Welded or seamless steel tubes for water, sewage and gas |  |  |  |
| JIS G Alloy steel pipes ASTM A335/ Spec. for seamless ferritic alloy steel pipe for high-temperature 3458 A335 M-92a service BS 3604/1-90 Spec. for seamless and electric resistance welded tubes |  |  |  |
| DIN 17175-79 Seamless tubes of high-temperature steels; technical conditions of delivery |  |  |  |
| DIN 17177-79 Electrically resistance of induction welded steel tubes for elevated temperature; technical terms of delivery |  |  |  |
| ISO 2604/2-75 Steel products for pressure purposes - quality requirements - Part II: Wrought seamless tubes |  |  |  |
| JIS G ISO 2604/3-75 Steel products for pressure purposes - quality requirements - 3458 Part III: Electric resistance and induction - welded tubes |  |  |  |
| JIS G ASTM A312/ 3459 A312 M-92a Spec. for seamless and welded austenitic stainless steel pipe |  |  |  |
| ASTM A358/ Spec. for electric-fusion-welded austenitic chromium-nickel alloy A358 M-92 steel pipe for high-temperature service |  |  |  |
| ASTM A376/ Spec. for seamless austenitic steel pipe for high-temperature A376 M-91 central-station service |  |  |  |
| ASTM A790/ Spec.for seamless and welded ferritic/austenitic stainless steel A790 M-91 pipe |  |  |  |
| BS 3605-92 Steel pipes and tubes for pressure purposes. Austenitic stainless steel DIN 17455-85 Welded circular tubes of stainless steels for general requirements |  |  |  |
| DIN 17456-85 Seamless circular tubes of stainless steels for general requirements |  |  |  |
| DIN 17457-85 Welded circular tubes of austenitic stainless steels for special requirements |  |  |  |
| DIN 17458-85 Seamless circular tubes of austenitic stainless steels for special requirements |  |  |  |
| JIS G Steel pipes for low ASTM A333/ Spec. for seamless and welded steel pipe for low temperature 3460 temperature A333 M-91 a service service |  |  |  |
| BS 3603-91 Steel pipes and tubes for pressure purposes, carbon and alloy steel: low temperature duties |  |  |  |
|  | DIN 17174-85 |  | Welded steel tubes for low temperature |
| DIN 17173-85 Seamless steel tubes for low temperatures |  |  |  |

info@persis-intl.com

| ISO 2604/2-75 |  |  |  | Steel products for pressure purposes - quality requirements - Part II: Wrought seamless tubes |
| --- | --- | --- | --- | --- |
| ISO 2604/3-75 |  |  |  | Steel products for pressure purposes - quality requirements - Part III: Electric resistance and induction - Welded tubes |
| JIS G 3468 | Arc welded large diameter stainless steel pipes | ASTM A358/ A358 M-92 |  | Spec. for electric-fusion-welded austenitic chromium-nickel alloy steel pipe for high-temperature service |
|  |  | ASTM A409/ A409 M-92 |  | Spec.for welded large outside diameter light-wall austenitic chromium-nickel alloy steel pipe for corrosive or high- temperature service |
|  |  | BS 3605-92 DIN 17455-85 |  | Seamless and welded austenitic stainless steel pipes and tubes for pressure purposes Ditto |
|  |  | DIN 17457-85 |  | Ditto |
|  |  | ISO 2604/5-78 |  | Steel products for pressure purposes - quality requirements. Part V: Longitudinally welded austenitic stainless steel tubes |
| JIS G 3461 | Carbon steel coiler and heat exchanger tubes | ASTM A178/ A178 M-90a |  | Spec. for electric-resistance-welded carbon steel boiler tubes |
|  |  | ASTM A179/ A179 M-90a |  | Spec. for seamless cold-drawn low-carbon steel heat exchanger and condenser tubes |
|  |  | ASTM A192/ A192 M-91 |  | Spec. for seamless carbon steel boiler tubes for high pressure service |
|  |  | ASTM A210/ A210 M-91 |  | Spec. for seamless medium-carbon steel boiler and superheater tubes |
|  |  | ASTM A214/ A214 M-90a |  | Spec. for electric-resistance welded carbon steel heat-exchanger and condenser tubes |
|  |  | ASTM A226/ A226 M-90a |  | Spec. for electric-resistance-welded carbon steel boiler and super-heater tubes for high-pressure service |
|  |  | BS 3059/1-87, 90 BS 3606-92 | /2- | Steel boiler and superheater tubes Steel tubes for heat exchangers |
| JIS G 3461 |  | DIN 17175-79 |  | Seamless steel tubes, for elevated temperature, technical terms of delivery |
|  |  | DIN 17177-79 |  | Electrically resistance of induction welded steel tubes for elevated temperature; technical terms of delivery |
|  |  | ISO 2604/2-75 |  | Steel products for pressure purposes - quality requirement - Part II: Wrought seamless tubes |
|  |  | ISO 2604/3-75 |  | Steel products for pressure purposes - quality requirements – - Part III: Electric resistance and induction - Welded tubes |
| JIS G 3462 | Alloy steel boiler and heat exchanger tubes | ASTM A199/ A199 M-92 |  | Spec. for seamless cold-drawn intermediate alloy-steel heat- exchanger and condenser tubes |
|  |  | ASTM A209/ A209 M-91 |  | Spec. for seamless carbon-molybdenum alloy-steel boiler and superheater tubes |
|  |  | ASTM A213/ A213 M-92 |  | Spec. for seamless ferritic and austenitic alloy-steel boiler, superheater, and heat exchanger tubes |
|  |  | ASTM A250/ A250 M-91 |  | Spec. for electric-resistance-welded carbon-molybdenum alloy- steel boiler, and superheater tubes |
|  |  | ASTM A423/ A423 M-91 BS 3059/2-90 |  | Spec. for seamless and electric welded low alloy-steel tubes Steel boiler and superheater tubes |
|  |  | BS 3606-92 |  | Steel tubes for heat exchangers |
|  |  | DIN 17175-79 |  | Seamless steel tubes for elevated temperatures; technical conditions of delivery |
|  |  | DIN 17177-79 |  | Electrically resistance of induction welded steel tubes for elevated temperature; technical terms of delivery |
|  |  | ISO 2604/2-75 |  | Steel products for pressure purposes - quality requirement, Part II: Wrought seamless tubes |
|  |  | ISO 2604/3-75 |  | Steel products for pressure purposes - quality requirement, Part III: Electric resistance and induction - Welded tubes |
| JIS G 3463 | Stainless steel boiler and heat exchanger tubes | ASTM A213/ A213 M-92 |  | Spec. for seamless ferritic and austenitic alloy-steel boiler, superheater, and heat exchanger tubes |
|  |  | ASTM A249/ A249 M-92 |  | Spec. for welded austenitic steel boiler, superheater, heat- exchanger, and condenser tubes |

info@persis-intl.com

|  |  | ASTM A268/ A268 M-91 | Spec. for seamless and welded ferritic stainless steel tubing for general service |
| --- | --- | --- | --- |
|  |  | ASTM A269-92 | Spec. for seamless and welded austenitic stainless tubing for general service |
|  |  | ASTM A789/ A789 M-90 BS 3059/2-90 | Spec. for seamless and welded ferritic austenitic stainless steel tubing for general service Steel boiler and superheater tubes |
|  |  | BS 3606-92 | Steel tubes for heat exchangers |
|  |  | DIN 17455-85 | Welded circular tubes of stainless steels for general requirements |
|  |  | DIN 17456-85 | Seamless circular tubes of stainless steels for general requirements |
|  |  | DIN 17457-85 | Welded circular tubes of austenitic stainless steels for special requirements |
|  |  | DIN 17458-85 | Seamless circular tubes of austenitic stainless steels for special requirements |
|  |  | ISO 2604/2-75 | Steel DINs for pressure purpose - quality requirements - Part II: Wrought seamless tubes |
|  |  | ISO 2604/3-75 | Steel products for pressure purpose - Quality requirements - Part III: Electric resistance and induction - Welded tubes |
|  |  | ISO 2604/5-78 | Steel products for pressure purposes - Quality requirements Part V: Longitudinally welded austenitic stainless steel tubes |
| JIS G 3464 | Steel heat exchanger tubes for low temperature service | ASTM A334/ A334 M-91 | Spec. for seamless and welded carbon and alloy-steel tubes for low-temperature service |
|  |  | BS 3603-91 | Steel pipes and tubes for pressure purposes. Carbon and alloy- steel: low temperature duties |
|  |  | DIN 17174-85 | Welded steel tubes for low temperature |
|  |  | DIN 17173-85 | Seamless steels tubes for low temperatures |
|  |  | ISO 2604/2-75 | Steel products for pressure purposes - Quality requirements - Part II: Wrought seamless tubes |
|  |  | ISO 2604/3-75 | Steel products for pressure purposes - Quality requirements - Part III: Electric resistance and induction - Welded tubes |
| JIS G 3467 | Steel tubes for fired heater | ASTM A161-91 | Spec. for seamless low-carbon and carbon-molybdenum steel still tubes for refinery service |
|  |  | ASTM A200-91 | Spec. for seamless intermediate alloy-steel still tubes for refinery service |
|  |  | ASTM A271-91 | Spec. for seamless austenitic chromium-nickel steel still tubes for refinery service |
| JIS G3444 | Carbon steel tubes for general structural purposes | ASTM A500-90a | Spec. for cold-formed welded and seamless carbon steel structural tubing in rounds and shapes |
|  |  | ASTM A501-89 BS 1139(1.1)-90 | Spec. for hot-formed welded and seamless carbon steel structural tubing Spec. for steel tubes |
|  |  | DIN 17120-84 | Welded circular steel tubes for structural steel-work |
|  | DIN 17121-84 |  | Seamless circular steel tubes for structural steel-work |
|  |  | DIN 17123-86 | Welded circular tubes of fine grain steels for engineering purposes |
|  |  | DIN 17124-86 | Seamless circular tubes of fine grain steel for engineering purposes |
| JIS G 3445 | Carbon steel tubes for machine structural purposes | ASTM A512-91 | Spec. for cold-drawn butt-weld carbon steel mechanical tubing |
| JIS G 3472 | Electric resistance welded carbon steel tubes for automobile structural purposes | ASTM A513-91a | Spec. for electric-resistance-welded carbon and alloy-steel mechanical tubing |
|  |  | ASTM A519-90 | Spec. for seamless carbon and alloy-steel mechanical tubing |
| JIS G 3473 | Carbon steel tubes | BS 1717-89 | Spec. for steel tubes for cycle and motorcycle purposes |
|  | for cylinder barrels |  |  |
| JIS G | Alloy-steel tubes | ASTM A519-90 | Spec. for seamless carbon and alloy-steel mechanical tubing |

info@persis-intl.com

| 3441 | for structural purposes |  |  |
| --- | --- | --- | --- |
|  |  | BS 1717-83 | Spec. for steel tubes for cycle and motorcycle purposes |
| JIS G 3446 | Stainless steel tubes for structural purposes | ASTM A511-90 | Spec. for seamless stainless steel mechanical tubing |
| JIS G 3466 | Carbon Steel square pipes for general structural purposes | ASTM A500-90a | Spec. for cold-formed welded and seamless carbon steel structural tubing in rounds and shapes |
| JIS G 3447 | Stainless steel sanitary tubing | ASTM A270-90 | Spec. for seamless and welded austenitic stainless steel sanitary tubing |
| JIS G 4903 | Seamless nickel- chromium-iron alloy pipes | ASTM B167-93 | Spec. for nickel-chromium-iron alloy (UNS No. 6600) seamless pipe and tube |
|  |  | ASTM B 407-93 | Spec. for nickel-iron-chromium alloy seamless pipe and tube |
|  |  | ASTM B 423-90 | Spec. for nickel-iron chromium-molybdenum-copper alloy (UNS No. 8825) seamless pipe and tube |
| JIS G 4904 | Seamless nickel- chromium-iron alloy heat exchanger tubes | ASTM B 163-93 | Spec. for seamless nickel and nickel alloy condenser and heat- exchangers tubes |
|  |  | ASTM B167-93 | Spec. for nickel-chromium-iron alloy (UNS No. 6600) seamless pipe and tube |
|  |  | ASTM B407-93 | Spec. for nickel-iron-chromium alloy seamless pipe and tube |
| JIS A5525 | Steel pipe piles | ASTM B423-90 ASTM A252-90 | Spec. for nickel-iron-chromium-molybdenum-copper alloy (UNS No. 8825) seamless pipe and tube |
|  |  |  | Spec. for welded and seamless steel pipe piles |
| JIS C8305 | Rigid steel conduit | BS 31-40(88) | Steel conduit and fitting for electrical wiring |
|  |  | ANSI C80.1-90 | Zinc coated rigid steel conduit |
|  |  | ANSI C80.3-83 | Enameled rigid steel conduit |
|  |  | UL*6-81 | Rigid metallic conduit |
| Wires & Wire Products |  |  |  |
| JIS G 3521 | Hard drawn steel wire | ASTM A227/ A227 M-91 ASTM A407-90 | Spec. for hard-drawn steel spring wire Spec. for hard-drawn steel wire for coiled-type springs |
|  |  | ASTM A417-90 | Spec. for hard-drawn steel wire for zig-zag, square-formed and sinuous-type upholstery spring units |
|  |  | ASTM A510-91 | Spec. for general requirements for wire rods and coarse round wire, carbon steel |
|  |  | ASTM A510 M-91 | Spec. for general requirements for wire rods and coarse round wire, carbon steel (Metric) |
|  |  | ASTM A679/ A679 M-91 BS 2453-73 | Spec. for high tensile strength, hard-drawn steel wire for mechanical springs Steel wire for spokes |
|  |  | BS 2763-82 | Round steel wire for ropes |
|  | BS 4637-70 |  | Carbon steel wire for coiled springs (bedding and soating) |
|  |  | BS 4638-70 | Carbon steel wire for zig-zag and square-form springs |
|  |  | BS 5216-91 | Patented cold drawn carbon steel wire for mechanical springs |
|  |  | DIN 177-88 | Round steel wire, cold drawn; dimensions, tolerances, weights |
|  |  | DIN 2076-84 | Round spring wire |
|  |  | DIN 2078-90 | Steel wires for wire ropes |
|  |  | DIN 17223/1-84 | Round spring steel wire, quality specifications, patented drawn spring wire made of unalloyed steels |
|  |  | ISO 2232-90 | Spec. for drawn wire for general purpose non-alloy steel wire ropes |
|  |  | ISO 6984-90 | Unalloyed steel wires for stranded wire ropes for mine-hoisting |
| JIS G 3522 | Piano wire | ASTM A228/ A228 M-91 | Spec. for music spring quality steel wire |
|  |  | BS 5216-91 DIN 2076-84 | Spec. for patented cold drawn carbon steel wire for mechanical springs Spring steel wire, round; patended and drawn spring-hard |
| DIN 17223/1-84 |  |  | Round steel wire for springs, patented cold drawn, carbon steel wire for springs |

info@persis-intl.com

| JIS G 3525 | Wire ropes | ASTM A603-88 Spec. for zinc-coated steel structural wire rope |  |
| --- | --- | --- | --- |
| BS 302-87 Wire ropes for cranes, excavators and general engineering purposes |  |  |  |
| DIN 2078-90 Steel wires for wire ropes |  |  |  |
| ISO 2232-90 Spec. for drawn wire for general purpose non-alloy steel wire ropes ISO 2408-85 Steel wire ropes for general purposes - Characteristics |  |  |  |
| ISO 3108-74 |  |  | Steel wire ropes for general purposes - determination of actual breaking load |
|  | ISO 3178-88 |  | Steel wire ropes for general purposes - terms of acceptance |
| ISO 4101-83 Drawn steel wire for elevator ropes |  |  |  |
| ISO 4344-83 Steel wire ropes for lifts |  |  |  |
| ISO 8369-86 Large diameter steel wire ropes |  |  |  |
|  | ISO 6984-90 |  | Unalloyed steel wires for stranded wire ropes for mine hoisting |
| JIS G 3532 | Iron wires | ASTM A82-90 Spec. for cold-drawn steel wire for concrete reinforcement |  |
| ASTM A510-91 Spec. for general requirements for wire rods and coarse round wire, carbon steel |  |  |  |
| ASTM A510 M-91 Spec. for general requirements for wire rods and coarse round wire, carbon steel (Metric) ASTM A641-92 Spec. for zinc-coated (galvanized) carbon steel wire |  |  |  |
| ASTM A641M-91 Spec. for zinc-coated (galvanized) carbon steel wire (Metric) |  |  |  |
| ASTM A817-92 Spec. for metallic-coated steel wire for chain link fence fabric |  |  |  |
| ASTM A824-92 Spec. for metallic-coated steel marcelled tension wire for use with chain link fence |  |  |  |
| BS 443-82 Spec. for testing zinc coating on steel wire and for quality requirements |  |  |  |
| BS 1052-80 Mild steel wire for general engineering purposes |  |  |  |
|  | BS 4102-90 |  | Steel wire for fences |
| BS 4482-85 Hard drawn mild wire for the reinforcement of concrete |  |  |  |
| DIN 177-88 Round steel wire, cold drawn; dimensions, tolerances, weights |  |  |  |
| DIN 1548-79 Zinc coating on round steel wires |  |  |  |
| JIS G 3533 | Barded wires | ASTM A121-92 Spec. for zinc-coated (galvanized) steel barbed wire BS 4102-90 Steel wire for fences |  |
| JIS G 3534 | Galvanized low carbon steel wire strand | ASTM A475-89 | Spec. for zinc-coated steel wire |
|  |  | BS 183-72 | General purpose galvanized steel wire strand |
| JIS G3536 | Uncoated stress- relieved steel wire and strand for prestressed concrete | ASTM A416-90 Spec. for uncoated seven-wire stress-relieved strand for prestressed concrete |  |
| ASTM A421-91 Spec. for uncoated stress-relieved wire for prestressed concrete |  |  |  |
| ASTM A779-90 Spec. for steel strand, seven wire, uncoated, compacted, stress- relieved for prestressed concrete |  |  |  |
| BS 5896-80 Specification for high tensile steel wire strand for the prestressing of concrete |  |  |  |
| Prestressed concrete; structural members made of normal-weight DIN 4227/1-88 concrete, with limited concrete tensile stresses or with concrete tensile stresses |  |  |  |
| JIS G 3537 | Galvanized steel wire strands | ASTM A363-89 Spec. for zinc-coated overhead ground wire strand ASTM A475-89 Spec. for zinc-coated steel wire strand |  |
| ASTM A586-92 Spec. for zinc-coated parallel and helical steel wire structural strand |  |  |  |
| BS 183-72 General purpose galvanized steel wire strand |  |  |  |
| JIS G 3538 | Hard drawn steel wire for prestressed concrete | ASTM A648-90 Spec. for steel wire, hard drawn for prestressing concrete pipe |  |
|  |  | ASTM A821-90 Spec. for steel wire, hard drawn for prestressing concrete tanks |  |

info@persis-intl.com

|  |  | by redrawing |  |
| --- | --- | --- | --- |
|  |  | BS 5896-80 | Spec. for high tensile steel wire strand for the prestressing of concrete |
| JIS G 3539 | Carbon steel wires for cold heading and cold forging | BS 3111/1-87 DIN 1654/1-89 | Steel wire for cold forged high tension bolts and similar components Steel for cold heading and cold extruding, general |
| DIN 1654/2-89 |  |  | Steel for cold heading and cold extruding, killed unalloyed steels not intended for heat treatment |
|  |  | DIN 1654/3-89 | Steel for cold heading and cold extruding , case hardening steels |
|  |  | DIN 1654/4-89 ISO 4954-93 | Steel for cold heading and cold extruding, steels for quenching and tempering Steels for cold heading and cold extruding |
| JIS G 3541 | Galvanized low carbon steel wire for armouring cables | ASTM A 411-86 BS 1441-69 | Spec. for zinc-coated (galvanized) low-carbon steel armor wire Galvanized steel wire for armouring submarine cables |
|  |  | BS 1442-69 | Galvanized mild steel wire for armouring cables |
| JIS G 3543 | Polyvinyl chloride coated color steel wires | ASTM F 668-91 BS 4102-90 | Spec. for PVC-coated steel chain-link fence fabric Steel wire for fences |
|  |  | DIN 3036-78 | Plastic coated steel wires |
| JIS G 3544 | Hot dip aluminum coated steel wire | ASTM A 474-86 | Spec. for aluminum-coated steel wire strand |
|  |  | ASTM A 491-92 | Spec. for aluminum-coated steel chain-link fence fabric |
|  |  | ASTM A584-92 | Spec. for aluminum-coated steel woven wire fence fabric |
|  |  | ASTM A585-92 | Spec. for aluminum-coated steel barbed wire |
|  |  | ASTM A809-91 | Spec. for aluminized carbon steel wire |
|  | ASTM A817-92 |  | Spec. for metallic-coated steel wire for chain-link fence |
| ASTM A824-92 |  |  | Spec. for metallic-coated steel marcelled tension wire for use with chain-link fence |
| ASTM B341-88 |  |  | Spec. for aluminized steel core wire for aluminum conductors (ACSR/AZ) |
| ASTM B341M-88 |  |  | Spec. for aluminum-coated (aluminized) steel core wire for aluminum conductors, steel reinforced (ACSR/AZ) metric |
|  | ASTM F 668-91 |  | Spec. for PVC-coated steel chain-link fence fabric |
| JIS G 3551 | Welded wire mesh | ASTM A185-90 | Spec. for welded steel wire fabric for concrete reinforcement |
|  |  | BS 4483-85 | Steel fabric for the reinforcement of concrete |
| JIS G 3552 | Chain link wire netting | ASTM A392-91 | Spec. for zinc-coated steel chain-link fence fabric |
|  |  | ASTM F 573-89 | Spec. for residential zinc-coated steel chain-link fence fabric |
|  |  | ASTM F668-91 | Spec. for PVC-coated steel chain-link fence fabric |
| JIS G 3554 | Hexagonal wire netting | BS 1485-83 | Spec. for zinc-coated hexagonal steel wire netting |
| JIS G 3560 | Oil tempered carbon steel spring wire | ASTM A229/ A229 M-91 | Spec. for oil-tempered steel wire for mechanical springs |
|  |  | BS 2803-80 | Oil hardened and tempered steel wire for springs for general engineering purposes |
|  |  | DIN 17223/2-90 | Round spring wire, quality specification; quenched and tempered spring wire and quenched and tempered valve spring wire made of unalloyed steels |
| JIS G 3561 | Oil tempered carbon steel valve spring quality wire | ASTM A230/ A230 M-91 | Spec. for oil-tempered carbon valve spring quality steel wire |
|  |  | BS 2803-80 | Oil hardened and tempered steel wire for springs general engineering purposes |
|  |  | DIN 17223/2-90 | Round spring wire, quality specifications; quenched and tempered spring wire and quenched and tempered valve spring wire made of unalloyed steels |
| JIS G 3565 | Oil tempered chromium | ASTM A231/ A231 M-91 | Spec. for chromium-vanadium alloy steel spring wire |

info@persis-intl.com

| JIS G 5101 | Carbon steel castings | ASTM A27/A27 M-91 | Spec. for mild-to medium-strenght carbon-steel casting for general application |
| --- | --- | --- | --- |
|  | BS 3100-91 |  | Steel castings for general engineering purposes |
|  |  | DIN 1681-85 | Cast steel (steel castings) |
|  |  | ISO 3755-90 | Cast steels for general engineering purposes |
|  |  | NF A32-051 | Foundry products – Castings – general purpose cast steels |
| JIS G 5102 | Steel castings for ASTM A216/ welded structure A216 M-89 |  | Spec. for carbon-steel castings suitable for fusion welding for high-temperature service |
| JIS G 5111 | High tensile strength carbon steel castings and low alloy steel castings for structural purposes | ASTM A148/ A148 M-90 | Spec. for high-strenght steel casting for structural purposes |
|  |  | BS 3100-91 | Steel castings for general engineering purposes (Low alloy steel castings for use at elevated temperatures)(1-1/2 per cent manganese steel castings) |
|  |  | NF A32-054 | Foundry products – Unalloyed and low alloy structural cast steels suitable for heat treatment |
| JIS G 5121 | Stainless steel castings | ASTM A743/ A743 M-92a | Spec. for castings, Fe-Cr, Fe-Cr-Ni, and nickel-base corrosion- resistant for general application |
|  |  | ASTM A744/ A744 M-91a | Spec. for castings, Fe-Cr-Ni and nickel-base corrosion-resistant for severe service |
|  |  | ASTM A351/ A351 M-91b | Spec. for austenitic steel castings for high- temperature service |
|  |  | BS 3100-91 | Steel castings for general engineering purposes(13 per cent chromium steel castings for resistance to corrosion)(Austenitic chromium-nickel steel castings for resistance to corrosion) |
|  |  | DIN 17445-84 | (Austenitic chromium-nickel-molybdenum steel castings for resistance to corrosion) Stainless steel castings; quality specifications |
|  |  | NF A 32-056 | Foundry products - Austenitic and austenoferric stainless steels |
|  |  | ASTM A 747/ A747 M-89 | Spec. for stainless precipitation hardening steel castings |
| JIS G 5122 | Heat resisting steel castings | ASTM A297/ A297 M-89 | Spec. for steel castings, Fe-Cr and Fe-Cr-Ni, heat resistant, for general application |
|  |  | ASTM A351/ A351M-91b | Spec. for steel castings, austenitic, for high-temperature service |
|  |  | ASTM A447/ A447M-87 | Spec. for chromium-nickel-iron alloy castings (25-12 class) for high-temperature service |
|  |  | BS 3100-91 | Steel castings for general engineering purposes(Alloy steel castings for use at high temperatures) |
|  |  | NF A32-057 | Foundry products - Heat resistant cast steel grades and related alloys |
| JIS G 5131 | High manganese steel castings | ASTM A128/ A128 M-90 | Spec. for austenitic manganese-steel castings |
| JIS G | Steel castings for | BS 3100-91 ASTM A216/ | Steel castings for general engineering purposes (Austenitic manganese steel casting) |
|  |  |  | Spec. for steel castings, carbon suitable for fusion welding for |

vanadium alloy

steel valve spring quality wire

ASTM A232/

A232 M-91

Spec. for chromium-vanadium steel valve spring quality wire

BS 2803-80	Oil hardened and tempered steel wire for spring for general engineering purposes

JIS G

3566

Oil tempered

chromium silicon	ASTM A401/

alloy steel valve

spring quality wire

A401 M-91

Spec. for chromium-silicon alloy steel spring wire

BS 2803-80	Oil hardened and tempered steel wire for spring for general engineering purposes

JIS G

3567

Oil tempered

silicon manganese ASTM A229/ alloy steel spring	A229 M-91 wires

Spec. for steel wire, oil tempered for mechanical springs

Castings and Forgings

info@persis-intl.com

| 5151 | high temperature and high pressure service | A216M-89 | high-temperature service |
| --- | --- | --- | --- |
|  |  | ASTM A389/ A389M-89 | Spec. for steel castings, alloy, specially heat-treated for pressure- containing parts suitable for high temperature service |
|  |  | ASTM A356/ A356 M-92 | Spec. for heavy-walled carbon and low alloy steel castings for steam turbines |
|  |  | ASTM A217/ A217 M-91 | Spec. for alloy steel castings for pressure-containing parts suitable for high-temperature service |
|  |  | BS 3100-91 | Steel castings for general engineering purposes (Chromium-molybdenum steel castings) |
|  |  | DIN 17245-87 | Ferritic steel castings creep resistant at elevated temperatures |
|  |  | NF A 32-055 | Castings - Weldable cast steels for boilers and pressure vessels |
| JIS G 5152 | Steel castings for low temperature and high pressure service | ASTM A 352/ A352 M-89 | Spec. for ferritic and martensitic steel castings for pressure- containing parts suitable for low-temperature service |
|  |  | ASTM A757/ A757M-90 | Spec. for steel castings, ferritic and martensitic for pressure- containing and other applications for low-temperature service |
|  |  | BS 3100-91 NF A 32-053 | Steel castings for general engineering purposes (Ferritic steel castings for use at low temperatures) Foundry products - cast steel grades for use at low temperatures |
| JIS G 5201 | Centrifugally cast steel pipes for welded structure | (ASTM A362-63) | Spec. for iron-chrnmium and iron-chromium-nickel alloy tubular centrifugally castings for general applications |
|  |  | BS 3100-91 | Steel castings for general engineering purposes |
| JIS G 5202 | Centrifugally cast steel pipes for high temperature and high pressure service | ASTM A 426-92 | Spec. for centrifugally cast ferritic alloy steel pipe for high- temperature service |
| JIS G 5501 | Gray iron castings | ASTM A48-92 BS 1452-90 | Spec. for gray iron castings Grey iron castings |
|  |  | (DIN 1691-85) | Cast iron with lameller graphite (gray cast iron) |
|  |  | ISO 185-88 | Grey cast iron-classification |
|  |  | NF A 32-101 | Foundry products - Lamellar graphite cast iron castings |
| JIS G 5502 | Spheroidal graphite iron castings | ASTM A536-84 | Spec. for ductile iron castings |
|  |  | BS 2789-85 | Iron castings with spheroidal or nodular graphite |
|  |  | (DIN 1693-77) | Cast iron with spheroidal graphite |
|  |  | GOCT 7293-85 | High strength cast iron mouldings with spherical graphite |
|  |  | ISO 1083-87 | Spheroidal graphite or nodular graphite cast iron |
|  | NF A 32-201 |  | Foundry products - Spheroidal graphite cast iron castings |
| JIS G 5510 | Austenitic iron castings | ASTM A436-84 ASTM A439-83 | Spec. for austenitic grey iron castings Spec. for austenitic ductile iron castings |
|  |  | ASTM A571-84 | Spec. for austenitic ductile iron castings for pressure-containing parts suitable for low-temperature service |
|  |  | ISO 2892-73 | Austenitic cast iron |
|  |  | BS 3468-86 | Austenitic cast iron |
|  |  | DIN 1694-81 | Austenitic cast iron |
|  |  | NF A32-301 | Austenitic cast iron |
| JIS G5526 | Ductile iron pipes | ISO 2531-91 | Ductile iron pipes, fittings and accessories for pressure pipelines |
| JIS G5527 | Ductile iron fittings | ISO 2531-91 | Ductile iron pipes, fittings and accessories for pressure pipelines |
| JIS G 5702 | Blackheart malleable iron castings | ASTM A47 M-90 | Spec. for malleable iron castings |
|  |  | ASTM A197 M-87 | Spec. for cupola malleable iron |
|  |  | BS 6681-86 | Spec. for malleable cast iron, blackheart |
|  |  | (DIN 1692-82) | Malleable cast iron; definition, properties, acceptance |
| JIS G | Whiteheart | BS 6681-96 | Spec. for malleable cast iron, whiteheart |

info@persis-intl.com

| 5703 | malleable iron castings |  |  |
| --- | --- | --- | --- |
|  |  | (DIN 1692-68) | Malleable cast iron; definition, properties, acceptance |
|  | NF A 32-701 |  | Foundry products - Whiteheart malleable iron castings |
| JIS G 5704 | Pearlitic malleable iron castings | ASTM A 220M-88 | Spec. for pearlitic malleable iron castings |
|  |  | BS 6681-86 | Spec. for malleable cast iron, pearlitic |
| JIS G 3201 | Carbon steel forgings | ASTM A668-91 | Spec. for carbon and alloy steel forgings for general industrial use |
|  |  | DIN 17103-89 | Weldable fine grain structural steel forgings |
|  |  | BS 29-76 | Spec. for carbon steel forgings above 150mm ruling section |
|  |  | NF A 36-612 | Structural forgings, non-alloyed steels |
| JIS G 3202 | Carbon steel forgings for pressure vessels | ASTM A105/ A105 M-92 | Spec. for forgings, carbon steel, for piping components |
|  |  | ASTM A181/ A181 M-90 | Spec. for forgings, carbon steel for general purpose piping |
|  |  | ASTM A266/ A266 M-92 | Spec. for forgings, carbon steel, for pressure vessel components |
|  |  | ASTM A508/ A508 M-92 | Spec. for Quenched and tempered vacuum-treated carbon and alloy steel forgings for pressure vessels |
|  |  | ASTM A541/ A541 M-92 | Spec. for steel forgings, carbon and alloy, quenched and tempered, for pressure vessel components |
|  |  | BS 1503-89 | Spec. for steel forgings (including semi-finished forged products) for pressure purposes |
|  |  | NF A 36-601-80 | Welded steel forgings for boilers and pressure vessels, carbon and carbon manganese steels |
| JIS G 3203 | Alloy steel forgings for pressure vessels for pressure vessels for high- temperature service | ASTM A182/ A182M-92 a | Spec. for forged or rolled alloy-steel, pipe flanges, forged fittings, and values and parts for high-temperature service |
|  |  | ASTM A336/ A336M-92 a | Spec. for steel forgings, alloy, for pressure and high-temperature parts |
|  |  | BS 1503-89 | Spec. for steel forgings (including semi-finished forged products) for pressure purposes |
|  |  | ISO 2604/1-75 | Steel products for pressure purposes - Quality requirements - Part I : Forgings |
|  |  | NF A36-602-88 | Welded steel forgings for boilers and pressure vessels, Mo-Mn-Mo and Cr-Mo alloy steel |
| JIS G 3204 | Quenched and tempered alloy steel forgings for pressure vessels | ASTM A508/ A508 M-92 | Spec. for quenched and tempered vacuum-treated carbon and alloy steel forgings for pressure vessels |
|  |  | ASTM A541/ A541 M-91 | Spec. for steel forgings, carbon and alloy, quenched and tempered, for pressure vessel components |
| JIS G 3205 | Carbon and alloy steel forgings for pressure vessels for low- temperature service | ASTM A350/ A350 M-92a | Spec. for forgings, carbon and low-alloy steel, requiring notch toughness testing for piping components |
|  |  | BS 1503-89 | Spec. for forgings (incl. semi-finished forged products) for pressure purposes |
|  |  | NF A 36-601-80 | Welded steel forgings for boilers and pressure vessels, carbon and carbon manganese steels |
| JIS G 3206 | High strength chromium molybdenum alloy steel forgings for pressure vessels under high- temperature service | ASTM A182/ A182 M-92 a | Forged or rolled alloy-steel pipe flanges, forged fittings and valves and parts for high temperature |
|  |  | ASTM A336/ A336 M-92a | Steel forgings, alloy, for pressure and high temperature service |
|  |  | ASTM A508/ | Quenched and tempered vacuum-treated carbon and alloy steel |

info@persis-intl.com

|  |  | A508 M-92 | forgings for pressure vessels |
| --- | --- | --- | --- |
|  |  | ASTM A541/ A541 M-91 | Steel forgings carbon and alloy, quenched and tempered for pressure vessel components |
| JIS G 3214 | Forged stainless steel flanges, fittings, valves and parts of pressure vessel for high- temperature service | ASTM A182/ A182 M-92 | Spec. for forged or rolled alloy-steel pipe flanges, forged fittings, and valves and parts for high-temperature service |
|  |  | ASTM A336/ A336 M-92 a | Spec. for steel forgings alloy, for pressure and high-temperature service |
|  |  | ASTM A705/ A705M-92 | Spec. for age-hardening stainless and heat-resisting steel forgings |
|  |  | BS 1503-89 | Spec. for steel forgings (including semi-finished forged products) for pressure purposes |
|  |  | ISO 2604/1-75 | Steel products for pressure purpose, quality requirements. Part 1: forgings |
|  |  | NF A 36-607-84 | Austenitic stainless steel parts obtained by flat die forging or drop forging for boiler and pressure vessels |
|  |  | ASTM A290-85 | Spec. for carbon and alloy steel forgings for rings for reduction gears |
|  |  | ASTM A291-92 | Spec. for carbon and alloy steel forgings for pinions and gears for reduction gears |
|  |  | BS 4670-71 | Spec. for alloy steel forgings |
| JIS G 3222 | Nickel chromium molybdenum steel forgings for general use | ASTM A 290-85 | Spec. for carbon and alloy steel forgings for rings for reduction gears |
|  |  | ASTM A 291-92 BS 4670-71 | Spec. for carbon and alloy steel forgings for pinions and gears for reduction gears Spec. for alloy steel forgings |

| Carbon and Alloy Steels for Machine Structural Use |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Std. No. Definition | Symbol | ISO683/1, 10, 11 | AISI / SAE | BS970 Part 1, 3 | DIN 17210, DIN EN 10083-1, -2 | NFA35-551, NF EN 10083- GOCT14959, 4543 1, 2 |  |
| JIS G 4051 Carbon Steels for machine structural use | S10C | C10 | 1010 | 040A10 045A10 045M10 | Ck10 C10 | XC10 | -- |
|  | S12C | -- | 1012 | 040A12 | -- | XC12 |  |
|  | S15C | C15E4 C15M2 | 1015 | 055M15 | Ck15 C15 | -- | -- |
|  | S17C |  | 1017 | -- | -- | XC18 |  |
|  |  |  |  |  | 1C22 | 1C22 |  |
|  | S20C | -- | 1020 | 070M20 | 2C22 | 2C22 | -- |
|  |  |  |  |  | 3C22 | 3C22 |  |
|  | S22C | -- | 1023 | -- | -- | -- | -- |
|  |  | C25 |  |  | 1C25 | 1C25 |  |
|  | S25C | C25E4 | 1025 | -- | 2C25 | 2C25 | -- |
|  |  | C25M2 |  |  | 3C25 | 3C25 |  |
|  | S28C | -- | 1029 | -- | -- | -- | 25G |
|  | S30C | C30 C30E4 C30M2 | 1030 | 080A30 080M30 | 1C30 2C30 3C30 | 1C30 2C30 3C30 | 30G |
|  | S33C | -- | -- | -- | -- | -- | 30G |
|  |  | C35 |  |  | 1C35 | 1C35 |  |
|  | S35C | C35E4 | 1035 | -- | 2C35 | 2C35 | 35G |
|  |  | C35M2 |  |  | 3C35 | 3C35 |  |
|  | S38C | -- | 1038 | -- | -- | -- | 35G |
|  | S40C | C40 C40E4 C40M2 | 1039 1040 | 080M40 | 1C40 2C40 3C40 | 1C40 2C40 3C40 | 40G |
|  | S43C | -- | 1042 1043 | 080A42 | -- | -- | 40G |
|  | S45C | C45 | 1045 | -- | 1C45 | 1C45 | 45G |
|  |  | C45E4 | 1046 |  | 2C45 | 2C45 |  |

C45M2	3C45	3C45

S48C	--	--	080A47  --	--	45G

S50C

C50 C50E4 C50M2

1049	080M50

1C50

2C50

3C50

1C50

2C50

3C50

50G

S53C	--	1050

1053

--	--	--	--

S55C

S58C

C55 C55E4 C55M2

C60 C60E4 C60M2

1055	070M55

1059	--

1060

1C55

2C55

3C55

1C60

2C60

3C60

1C55

2C55

3C55

1C60

2C60

3C60

--

60G

S09CK	--	--	045A10 045M10

Ck10	XC10	--

JIS G 4102 Nickel chromium steels

S15CK	--	--	--	Ck15	XC12

S20CK	--	--	--	--	XC18

SNC 236  --	--	--	--	--	40XH

SNC 415  --	--	--	--	--	--

SNC 631  --	--	--	--	--	30XH3A SNC 815  15NiCr13	--	655M13  --	--	--

SNC 836  --	--	--	--	--	--

JIS G 4103 Nickel chromium

SNCM

20NiCrMo2

8615

8617

805A20

805M20

21NiCrMo2

20NCD2	--

molybdenum steels

220

20NiCrMoS2 8620

8622

805A22

805M22

21NiCrMoS2

JIS G 4103	SNCM240 41CrNiMo2

8637

--	--	--	--

SNCM 415

SNCM 420

SNCM 431

SNCM 439

SNCM

41CrNiMos2 8640

--	--	--	--	--	--

--	4320	--	--	--	20XH2M(20XHM)

--	--	--	--	--	--

--	4340	--	--	--	--

447	--	--	--	--	--	--

SNCM 616

SNCM

--	--	--	--	--	--

625	--	--	--	--	--	--

SNCM 630

SNCM

--	--	--	--	--	--

815	--	--	--	--	--	--

JIS G 4104 Chromium steels  SCr 415  16MnCr5

16MnCrS5

SCr 420   20Cr4

20CrS4

--	--	--	16MC5	15X 15XA

5120	--	20Cr4	20MC5	20X

SCr 430   34Cr4

34CrS4

34Cr4

5130

5132

--	34Cr4 34CrS4

34Cr4

34CrS4

30X

SCr 435

SCr 440

34CrS4

37Cr4

37CrS4

37Cr4

37CrS4

41Cr4

41CrS4

5132	--	37Cr4

37CrS4

5140	530M40  41Cr4

41CrS4

37Cr4

37Cr4

41Cr4

41CrS4

35X

40X

SCr 445   --	--	--	--	--	--

JIS G 4105 Chromium

molybdenum steels	SCM 415  --	--	--	--	--	--

info@persis-intl.com

SCM 418 18CrMo4

18CrMoS4

--	--	--	--	20XM

info@persis-intl.com

Standard No.

Definition

Standard No.

Definition

|  | SCM 420 | -- | -- | 708M20 | -- | -- | 20XM |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | SCM 421 | -- | -- | -- | -- | -- | -- |
|  | SCM 430 | -- | 4131 | -- | -- | -- | 30XM 30XMA |
|  | SCM 432 | -- | -- | -- | -- | -- | -- |
|  | SCM 435 | 34CrMO4 34CrMoS4 | 4137 | -- | 34CrMo4 34CrMoS4 | 34CrMo4 34CrMoS4 | 35XM |
|  | SCM 440 | 42CrMo4 42CrMoS4 | 4140 4142 | 708M40 709M40 | 42CrMo4 42CrMoS4 | 42CrMo4 42CrMoS4 | -- |
|  | SCM 445 | -- | 4145 4147 | -- | -- | -- | -- |
|  | SCM 882 | -- | -- | -- | -- | -- | -- |
| JIS G 4106 Manganese steels and manganese chromium steels for machine structural use | SMn 420 | 22Mn6 | 1522 | 150M19 | -- | -- | -- |
|  | SMn 433 | -- | 1534 | 150M36 | -- | -- | 30G2 35G2 |
|  | SMn 438 | 36Mn6 | 1541 | 150M36 | -- | -- | 35G2 40G2 |
|  | SMn 443 | 42Mn6 | 1541 | -- | -- | -- | 40G2 45G2 |
|  | SMnC420 | -- | -- | -- | -- | -- | -- |
| JIS G 4106 | SMnC 443 | -- | -- | -- | -- | -- | -- |
| JIS G 4202 Aluminium chromium molybdenum steels | SACM 645 | 41CrAlMo74 | -- | -- | -- | -- | -- |
| JIS G 4052 Structural steels with specified hardenability bands | SMn 420H | 22Mn6 | 1522H | -- | -- | -- | -- |
|  | SMn 433H | -- | -- | -- | -- | -- | -- |
|  | SMn 438H | 36Mn6 | 1541H | -- | -- | -- | -- |
|  | SMn 443H | 42Mn6 | 1541H | -- | -- | -- | -- |
|  | SMnC 420H | -- | -- | -- | -- | -- | -- |
|  | SMnC 443H | -- | -- | -- | -- | -- | -- |
|  | SCr 415H | 16MnCr5 16MnCrS5 | -- | -- | -- | 16MC5 | 15X |
|  | SCr 420H | 20Cr4 20CrS4 | 5120H | -- | 20Cr4 | 20MC5 | 20X |
|  | SCr 430H | 34Cr4 34CrS4 | 5130H 5132H | -- | 34Cr4 34CrS4 | 34Cr4 34CrS4 | 30X |
|  |  | 34Cr4 |  |  |  |  |  |
|  | SCr 435H | 34CrS4 37Cr4 | 5135H | -- | 37Cr4 37CrS4 | 37Cr4 37CrS4 | 35X |
|  |  | 37CrS4 |  |  |  |  |  |
|  |  | 37Cr4 |  |  |  |  |  |
|  | SCr 440H | 37CrS4 41Cr4 | 5140H | -- | 41Cr4 41CrS4 | 41Cr4 41CrS4 | 40X |
|  |  | 41CrS4 |  |  |  |  |  |
|  | SCM 415H | -- | -- | -- | -- | -- | -- |
|  | SCM 418H | 18CrMo4 18CrMoS4 | -- | -- | -- | -- | -- |
|  | SCM 420H | -- | -- | 708H20 | -- | -- | -- |
|  | SCM 435H | 34CrMo4 34CrMoS4 | 4135H 4137H | -- | 34CrMo4 34CrMoS4 | 34CrMo4 34CrMoS4 | -- |
|  | SCM 440H | 42CrMo4 42cRMoS4 | 4140H 4142H | -- | 42CrMo4 42CrMoS4 | 42CrMo4 42CrMoS4 | -- |
|  | SCM | -- | 4145H | -- | -- | -- | -- |

info@persis-intl.com

|  |  | 445H |  | 4147H |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | SCM 822H | -- | -- | -- | -- | -- | -- |  |
|  |  | SNC 415H | -- | -- | -- | -- | -- | -- |  |
|  |  | SNC 631H | -- | -- | -- | -- | -- | -- |  |
|  |  | SNC 815H | 15NiCr13 | -- | 655H13 | -- | -- | -- |  |
|  |  | SNCM 220H | 20NiCrMo2 20NiCrMoS2 | 8617H 8620H 8622H | 805H17 805H20 805H22 | -- | 20NCD2 | -- |  |
|  |  | SNCM 420H | -- | 4320H | -- | -- | -- | -- |  |
| JIS G 4107 |  | SNB 5 | -- | 501 | -- | -- | -- | -- |  |
|  |  | SNB 7 | - | 4140 4142 4145 | 708M40 709M40 630- 860(1) | 42CrMo4(2) | -- | -- |  |
| Alloy steel bolting materials |  |  |  |  |  |  |  |  |  |
| for high temperature |  |  |  |  |  |  |  |  |  |
| services |  |  |  |  |  |  |  |  |  |
|  |  | SNB 16 | -- | -- | 670- 860(1) | 40CrMoV47(2) | 42CDV4(3) |  |  |
| JIS G 4108 Alloy steel bars for special |  | SNB 21-1 to 21-5 | -- | -- | 670- 860(1) | 40CrMoV47(2) | 42CDV4(3) |  |  |
|  |  | SNB 22-1 to 22-5 | -- | 4142H | -- | 42CrMo4(2) | -- | -- |  |
| application bolting materials |  |  |  |  |  |  |  |  |  |
|  |  | SNB 23-1 to 23-5 | -- | E 4340H | -- | -- | -- | -- |  |
|  |  | SNB 24-1 to 24-5 | -- | 4340 | -- | -- | -- | -- |  |
| Corrosion and heat-resisting Steels |  |  |  |  |  |  |  |  |  |
| Std. No., Symbol Definition |  | ISO | UNS | AISI | BS | DIN | NF | GOCT | EN |
| JIS G |  |  |  |  |  |  |  |  |  |
| 4303- 4305 SUS 201 Stainless |  | A-2 | S20100 | 201 |  |  | Z12CMN17- 07Az |  | X12CrMnNiN17-7-5 |
| steel bars |  |  |  |  |  |  |  |  |  |
| SUS 202 |  | A-3 | S20200 | 202 | 284S16 |  |  | 12X17G9AH4 | X12CrMnNiN18-9-5 |
| Hot rolled stainless steel SUS 301 sheets and plates, strips |  | 14 | S30100 | 301 | 301S21 | X12CrNil7 7 | Z11CN17-08 |  |  |
| Cold rolled |  |  |  |  |  |  |  |  |  |
| stainless |  |  |  |  |  |  |  |  |  |
| steel SUS 301L |  |  |  |  |  | X2CrNi18 7 |  |  |  |
| sheets and |  |  |  |  |  |  |  |  |  |
| plates, |  |  |  |  |  |  |  |  |  |
| strips |  |  |  |  |  |  |  |  |  |
| SUS 301J1 |  |  |  |  |  | X12CrNi7 7 |  |  |  |
| JIS G |  |  |  |  |  |  |  |  |  |
| 4308- |  |  |  |  |  |  |  |  |  |
| 4309 SUS302 Stainless |  | 12, H10(1) | S30200 | 302 | 302S25 |  | Z12CN18-09 | 12X18H9 | X9CrNi18-8 |
| steel wire |  |  |  |  |  |  |  |  |  |
| rods |  |  |  |  |  |  |  |  |  |
| SUS302B |  |  | S30215 | 302B |  |  |  |  |  |
| Stainless | SUS 303 | 17 | S30300 | 303 | 303S21 | X10CrNiS18 9 | Z8CNF18-09 |  | X8CrNiS18-9 |
| steel wires |  |  |  |  |  |  |  |  |  |
| JIS G |  |  |  |  |  |  |  |  |  |
| 4313- |  |  |  |  |  |  |  |  |  |
| 4315 Cold rolled stainless | SUS303Se SUS 304 | 17a 11 | S30323 S30400 | 303Se 304 | 303S41 304S31 | X5CrNi18 10 | Z7CN18-09 | 12X18H10E 08X18H10 | X4CrNi18-10 |
| steel strips |  |  |  |  |  |  |  |  |  |
| for springs |  |  |  |  |  |  |  |  |  |
| Stainless | SUS 304L | 10 | S30403 | 304L | 304S11 | X2CrNi19 11 | Z3CN19-11 | 03X18H11 | X2CrNi19-11 |

info@persis-intl.com

| steel wires for springs |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Stainless |  |  |  |  |  |  |  |  |  |
| steel wires |  |  |  |  |  |  |  |  |  |
| for cold heading | SUS 304N1 SUS 304N2 |  | S30451 S30452 | 304N |  |  | Z6CN-19-09Az |  |  |
| and cold |  |  |  |  |  |  |  |  |  |
| forging |  |  |  |  |  |  |  |  |  |
| JIS G |  |  |  |  |  |  |  |  |  |
| 4317- |  |  |  |  |  |  |  |  |  |
| 4320 Hot rolled stainless | SUS 304LN SUS 304J1 | 10N | S30453 | 304LN |  | X2CrNiN18 10 | Z3CN18-10Az |  | X2CrNiN18-10 |
| steel equal |  |  |  |  |  |  |  |  |  |
| leg angles |  |  |  |  |  |  |  |  |  |
| Cold finished stainless steel bars | SUS 304J2 |  |  |  |  |  |  |  |  |
| Stainless |  |  |  |  |  |  |  |  |  |
| steel |  |  |  |  |  |  |  |  |  |
| blooms and billets | SUS 304J3 SUS305 | 13 | S30431 S30500 | S30431 305 | 305S19 | X5CrNi18 12 | X5CrN18-12 |  | X4CrNi18-12 |
| for |  |  |  |  |  |  |  |  |  |
| forgings |  |  |  |  |  |  |  |  |  |
| Cold |  |  |  |  |  |  |  |  |  |
| formed stainless steel equal | SUS 305J1 SUS 309S | H14(1) | S30908 | 309S |  |  |  |  |  |
| leg angles |  |  |  |  |  |  |  |  |  |
|  | SUS310S | H15(1) | S31008 | 310S | 310S31 |  | Z8CN25-20 | 10X23H18 | X1CrNi25-21 |
|  | SUS 316 | 20,20a | S31600 | 316 | 316S31 | X5CrNiMo17 12 2X5CrNiMo17 13 3 | Z7CND17-12- 02 Z6CND18-12- 03 |  | X4CrNiMo17-12-2 X4CrNiMo17-13-3 |
|  |  |  |  |  |  | X2CrNiMo17 | Z3CND17-12- |  |  |
|  | SUS 316L | 19,19a | S31603 | 316L | 316S11 | 13 2 X2CrNiMo17 | 02 Z3CND17-13- | 03X17H14M2 | X2CrNiMo17-12-2 X2CrNiMo17-12-3 |
|  |  |  |  |  |  | 14 3 | 03 |  |  |
|  | SUS 316N |  | S31651 | 316N |  |  |  |  |  |
|  | SUS 316LN | 19N, 19aN | S31653 | 316LN |  | X2CrNiMoN17 12 2 X2CrNiMoN17 13 3 | Z3CND17-11Az Z3CND17-12Az |  | X2CrNiMoN17-11-2 X2CrNiMoN17-13-3 |
|  | SUS 316Ti |  | S31635 |  |  | X6CrNiMoTi17 12 2 | Z6CDNT17-12 |  | X6CrNiMoTi17-12- 2 |
|  | SUS 316J1 |  |  |  |  |  |  |  |  |
|  | SUS 316J1L |  |  |  |  |  |  |  |  |
|  | SUS 317 |  | S31700 | 317 | 317S16 |  |  |  |  |
|  | SUS 317L | 24 | S31703 | 317L | 317S12 | X2CrNiMo18 16 4 | Z3CND19-15- 04 |  | X2CrNiMo18-15-4 |
|  | SUS 317LN |  | 31753 |  |  |  | Z3CND19-14Az |  | X2CrNiMoN17-12-3 |
| SUS 317J1 |  |  |  |  |  |  |  |  |  |
| SUS 317J2 |  |  |  |  |  |  |  |  |  |
| SUS 317J3L |  |  |  |  |  |  |  |  |  |
|  | SUS 317J4L |  | N08367 |  |  |  |  |  |  |
|  | SUS 317J5L | A-4 | N08904 | N08904 |  |  | Z2NCDU25-20 |  | X1CrNiMoCuN25- 25-5 |
|  | SUS 321 | 15, H11(1) | S32100 | 321 | 321S31 | X6CrNiTi18 10 | Z6CNT18-10 | 08X18H10T | X6CrNiTi18-10 |
|  | SUS 347 | 16, H12(1) | S34700 | 347 | 347S31 | X6CrNiNb18 10 | Z6CNNb18-10 | 08X18H10 | X6CrNiNb18-10 |
|  | SUS 384 | D25(2) | S38400 | 384 |  |  | Z6CN18-16 |  |  |
|  | SUS XM7 | D26(2) | S30430 | 304Cu |  |  | Z6CNU18-10 |  | X6CrNiCu18-10-4 |
|  | SUS XM15J1 |  | S38100 |  |  |  | Z15CNS20-12 |  | X1CrNiSi18-15-4 |
|  | SUS 329J1 |  | S32900 | 329 |  |  |  |  |  |
|  | SUS 329J3L |  | S39240 | S31803 |  |  | Z3CNDU22- | X2CrNiMoN22-5-3 |  |

info@persis-intl.com

|  |  |  |  |  |  | 05Az |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SUS 329J4L |  | S39275 |  |  |  | Z3CNDU25- 07Az | X2CrNiMoCuN25-6- 3 |  |
|  | SUS 405 | 2 | S40500 | 405 | 405S17 | X6CrAl13 | Z8CA12 | 12X13IO | X6CrAl13 |
|  | SUS 410L |  |  |  |  |  |  |  |  |
|  | SUS 429 |  | S42900 | 429 |  |  |  |  |  |
|  | SUS 430 | 8,H4(1) | S43000 | 430 | 430S17 | X6Cr17 | Z8Cr17 | 12X17 | X6Cr17 |
|  | SUS430F | 8a | S43020 | 430F |  | X7CrMoS18 | Z8CF17 |  | X6CrMoS17 |
|  | SUS 430LX |  | S43035 |  |  | X6CrTi17, X6CrNb17 | Z4CT17 | X3CrTi17 |  |
|  | SUS 430J1L |  |  |  |  |  | Z4CNb17 | X3CrNb17 |  |
|  | SUS 434 | 9c | S43400 | 434 | 434S17 | X6CrMo17 1 | Z8CD17-01 |  | X6CrMo17-1 |
|  | SUS 436L |  | S43600 | 436 |  |  |  |  | X1CrMoTi16-1 |
| SUS 436J1L |  |  |  |  |  |  |  |  |  |
|  | SUS 444 | F1 | S44400 | 444 |  |  | Z3CDT18-02 | X2CrMoTi18-2 |  |
|  | SUS 447J1 | S44700 |  |  |  |  |  |  |  |
|  | SUS XM27 |  | S44625 |  |  |  | Z1CD26-01 |  |  |
|  | SUS403 |  | S40300 | 403 |  |  |  | 12X13 |  |
|  | SUS410 | 3 | S41000 | 410 | 410S21 | X10Cr13 | Z13C13 | 08X13 | X12Cr13 |
|  | SUS410S | 1 | S41008 | 410S | 403S17 | X6Cr13 | Z8C12 |  | X6Cr13 |
|  | SUS 410F2 |  |  |  |  |  |  |  |  |
|  | SUS 410J1 |  | S41025 |  |  |  |  |  |  |
|  | SUS 416 | 7 | S41600 | 416 | 416S21 |  | Z11CF13 | X12CrS13 |  |
|  | SUS 420J1 | 4 | S42000 | 420 | 420S29 | X20Cr13 | Z20C13 | 20X13 | X20Cr13 |
|  | SUS 420J2 | 5 | S42000 | 420 | 420S37 | X20Cr13 | Z33C13 | 30X13 | X80Cr13 |
|  | SUS 420F |  | S42020 | 420F |  |  | Z30CF13 |  | X29CrS13 |
| SUS 420F2 |  |  |  |  |  |  |  |  |  |
|  | SUS 429J1 |  |  |  |  |  |  |  |  |
|  | SUS 431 | 9 | S43100 | 431 | 431S29 | X20CrNi17 2 | Z15CN16-02 | 14X17H2 | X19CrNi17-2 |
|  | SUS 440A |  | S44002 | 440A |  |  | Z70C15 |  | X70CrMo15 |
|  | SUS 440B |  | S44003 | 440B |  |  |  |  |  |
|  | SUS 440C | A-1b | S44004 | 440C |  |  | Z100CD17 | 95X18 | X10CrMo17 |
|  | SUS 440F |  | S44020 | S44020 |  |  |  |  |  |
|  | SUS 630 | 1(3) | S17400 | S17400 |  |  | Z6CNU17-04 |  | X5CrNiCuNb16-4 |
|  | SUS 631 | 2(3) | S17700 | S17700 |  | X7CrNiAl17 7 | Z9CNA17-07 | 09X17H7IO | X7CrNiAI17-7 |
| JIS G 4311 to 4312 | SUH 31 | 5(4) |  |  | 331S42 |  |  | 45X14H14B2M X42CrNiW14-14 |  |
|  | SUH 35 | 8(4) |  |  | 349S52 |  | Z52CMN21-09 | 5X20G9AH4 |  |
| Heat- resisting steel bares | SUH36 | 9(4) | S63008 |  | 349S54 | X53CrMnNi219 |  |  |  |
| Heat- resisting steel sheets and plates | SUH 37 | 7(4) | S63017 |  | 381S34 |  |  |  |  |
|  | SUH 38 |  |  |  |  |  |  |  |  |
|  | SUH 309 | H14(1) | S30900 | 309 | 309S24 |  | Z12CN24-13 | 20X23H13 | X15CrNi23-13 |
|  | SUH 310 | H15(1) | S31000 | 310 | 310S24 |  | Z12CN25-20 | 20X25H20C2 |  |
|  | SUH 330 | H17(1) | N08330 | N08330 |  |  | Z12NCS35.16 |  |  |
|  | SUH 660 |  | S66286 |  |  |  |  |  |  |
|  | SUH 661 | 12(4) | R30155 |  |  |  |  |  |  |
|  | SUH 21 |  |  |  |  |  |  |  |  |
|  | SUH 409 | 1Ti,H1(1) | S40900 | 409 | 409S19 | X6CrTi12 |  |  |  |
|  | SUH 409L |  |  |  |  |  | Z3CT12 |  | X6CrTi12 |
|  | SUH 446 | H7(1) | S44600 | 446 |  |  | Z10C24 | 15X28 |  |
|  | SUH 1 | 1(4) | S65007 |  | 401S45 | X45CrSi93 | Z45CS9 |  |  |
|  | SUH 3 | 2(4) |  |  |  |  | Z40CSD10 |  |  |

info@persis-intl.com

| SUH 4 |  | 4(4) |  |  | 443S65 |  | Z80CSN20-02 | 40X10C2M |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SUH 11 |  |  |  |  |  |  |  | 40X9C2 | X45CrSi8 |
|  | SUH 600 |  |  |  |  |  |  | 20X12BMǼ |  |
|  | SUH 616 |  | S42200 |  |  |  |  |  |  |
| Tools Steels |  |  |  |  |  |  |  |  |  |
| Std. No., Definition |  | Symbol | ISO | AISI ASTM | BS | DIN VDEh | NF | GOCT |  |
| JIS G 4401 steels | Carbon tool | SK1 | TC140 | -- | -- | -- | Y2 140 | Y13 |  |
|  |  | SK2 | TC120 | W1-11 ?/font> | -- | -- | Y2 120 | Y12 |  |
|  |  | SK3 | TC105 | W1-10 | -- | C105W1 | Y1 105 | Y11 |  |
|  |  | SK4 | TC90 | W1-9 | -- | -- | Y1 90 | Y10 |  |
|  |  | SK5 | TC90/TC80 | W1-8 | -- | C80W1 | Y1 90,Y 180 | Y8G,Y9 |  |
|  |  | SK6 | TC80/TC70 | -- | -- | C80W1 | Y180,Y1 70 | Y8 |  |
| SK7 |  |  | -- | -- | -- | C70W2 | Y170 | Y7 |  |
| JIS G 4403 steels | High speed tool | SKH 2 | HS18-01-1 | T1 | BT1 | -- | Z 80WCV18- 04-01 | P18 |  |
|  |  | SKH 3 | HS18-1-5 | T4 | BT4 | S18-1-2-5 | Z 80WKCV18- 05-04-01 | -- |  |
|  |  | SKH 4 | HS18-0-1- 10 | T5 | BT5 | -- | Z80WKCV18- 10-04-02 | -- |  |
|  |  | SKH 10 | HS12-1-5-5 | T15 | BT15 | S12-1-4-5 | Z 160WKCV12- 05-05-04 | -- |  |
|  |  | SKH 51 | HS6-5-2 | M2 | BM2 | S6-5-2 | Z 85WDCV-06- 05-04-02 | -- |  |
|  |  | SKH 52 | -- | M3-1 | -- | -- | -- | -- |  |
|  |  | SKH 53 | HS6-5-3 | M3-2 | -- | S6-5-3 | Z 120WDCV06- 05-04-03 | -- |  |
|  |  | SKH 54 | -- | M4 | BM4 | -- | Z 130WDCV06- 05-04-04 | -- |  |
|  |  | SKH 55 | HS6-5-2-5 | -- | BM 35 | S6-5-2-5 | Z 90WDKCV06- 05-05-04-02 | P6M5K5 |  |
|  |  | SKH 56 | -- | M36 | -- | -- | -- | -- |  |
|  |  | SKH 57 | HS10-4-3- 10 | -- | BT42 | S10-4-3-10 | Z 130WKCDV10- 10-04-04-03 | -- |  |
|  |  | SKH 58 | HS2-9-2 | M7 | -- | -- | Z 100DCWV09- 04-02-02 | -- |  |
| JIS G 4404 | Alloy tool steels | SKH 59 SKS 11 | HS2-9-1-8 -- | M42 F2 | BM42 -- | S2-10-1-8 -- | Z 110DKCWV09- 08-04-02-01 -- | -- XB4 |  |
|  |  | SKS 2 | 105WG1 | -- | -- | 105WCr6 | 105WC13 | -- |  |
|  |  | SKS 21 | -- | -- | -- | -- | -- | -- |  |
| SKS 5 |  |  | -- | -- | -- | -- | -- | -- |  |
|  |  | SKS 51 | -- | L6 | -- | -- | -- | -- |  |
|  |  | SKS 7 | -- | -- | -- | -- | -- | -- |  |
|  |  | SKS 8 | -- | -- | -- | -- | Y2140C | 13X |  |
| SKS 4 |  |  | -- | -- | -- | -- | -- | -- |  |
|  |  | SKS 41 | -- | -- | -- | -- | -- | -- |  |
|  |  | SKS 43 | TCV105 | W2 | BW2 | -- | Y1 105V | -- |  |
|  |  | SKS 44 | -- | W2 | -- | -- | -- | -- |  |
| SKS 3 |  |  | -- | -- | -- | -- | -- | 9XBG |  |
|  |  | SKS 31 | -- | -- | -- | 105WCr6 | 105WC13 | XBG |  |
|  |  | SKS 93 | -- | -- | -- | -- | -- | -- |  |
|  |  | SKS 94 | -- | -- | -- | -- | -- | -- |  |
| SKS 95 |  |  | -- | -- | -- | -- | -- | -- |  |
|  |  | SKD 1 | 210Cr12 | D3 | BD3 | X210Cr12 | Z200C12 | X12 |  |
|  |  | SKD 11 | -- | D2 | BD2 | -- | Z160CDV12 | -- |  |

info@persis-intl.com

|  | SKD 12 | 100CrMoV5 | A2 | BA2 | -- | Z100CDV5 | -- |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | SKD 4 | 30WCrV5 | -- | -- | -- | Z32 WCV5 | -- |
|  | SKD 5 | 30WCrV9 | H21 | BH21 | -- | Z30 WCV9 |  |
|  | SKD 6 | -- | H11 | BH11 | X38CrMoV51 | Z 38 CDV5 | 4X5MǼC |
|  | SKD 61 | 40CrMoV5 | H13 | BH13 | X40 CrMoV51 | Z40 CDV5 | 4X5MǼ1C |
|  | SKD 62 | -- | H12 | BH12 | -- | Z35 CWDV5 | 3X3M3Ǽ |
| SKD 7 |  | 30CrMoV3 | H10 | BH10 | X32 CrMoV33 | 32 DCV28 | -- |
|  | SKD 8 | -- | H19 | BH19 | -- | -- | -- |
|  | SKT 3 | -- | -- | -- | -- | 55 CNDV4 | -- |
|  | SKT 4 | 55NiCrMoV2 | -- | BH224/5 | 55NiCrMoV6 | 55 NCDV7 | 5XGM |
| Steels for Special Purposes |  |  |  |  |  |  |  |
| JIS G 4801 Spring Steels | SUP 3 | -- | 1075 1078 | -- | -- | -- | 75,80 85 |
|  | SUP 6 | 59Si7 | -- | -- | -- | -- | 60C2 |
| SUP 7 |  | 59Si7 | 9260 | -- | -- | -- | 60C2G |
|  | SUP 9 | 55Cr3 | 5515 | -- | 55Cr3 | 55C3 | -- |
|  | SUP 9A | -- | 5160 | -- | -- | -- | -- |
|  | SUP 10 | 51CrV4 | 6150 | 735A51 735H51 | 50CrV4 | 50CV4 | X A50XTǼA |
|  | SUP 11A | 60CrB3 | 51B60 | -- | -- | -- | 50XGP |
|  | SUP 12 | 55SiCr63 | 9254 | 685A57 685H57 | 54SiCr6 | -- | -- |
|  | SUP 13 | 60CrMo33 | 4161 | 705A60 705H60 | -- | -- | -- |
| JIS G 4804 Resulphurized carbon steels | SUM 11 | -- | 1110 | -- | -- | -- | -- |
|  | SIM 12 | -- | 1108 | -- | -- | - | -- |
|  | SUM 21 | 9S20 | 1212 | -- | -- | -- | -- |
| SUM 22 |  | 11SMn28 | 1213 | 230M07 | 9SMn28 | S250 | -- |
|  | SUM 22L | 11SMnPb28 | 12L13 | -- | 9SMnPb28 | S250Pb | -- |
|  | SUM 23 | -- | 1215 | -- | -- | -- | -- |
|  | SUM 23L | -- | -- | -- | -- | -- | -- |
| SUM 24L |  | 12SMnPb35 | 12L14 | -- | 9SMnPb36 | S300Pb | -- |
|  | SUM 25 | 12SMn35 | -- | -- | 9SMn36 | S300 | -- |
|  | SUM 31 | -- | 1117 | -- | 15S10 | -- | -- |
|  | SUM 31L | -- | -- | -- | -- | -- | -- |
| SUM 32 |  | -- | -- | 210M15 | -- | (13MF4) | -- |
|  | SUM 41 | -- | 1137 | -- | -- | (35MF6) | -- |
|  | SUM 42 | -- | 1141 | -- | -- | (45MF6.1) | -- |
|  | SUM 43 | 44SMn28 | 1144 | 226M44 | -- | (45MF6.3) |  |
| JIS G 4805 High carbon chromium bearing steels | SUJ 1 | -- | 51100 | -- | -- | -- | -- |
|  | SUJ 2 | 1 | 52100 | 535A99 | 100Cr6 | 100C6 | ȁX15 |
|  |  |  | ASTM |  |  |  |  |
|  | SUJ 3 | 2 | A485 Grade- | -- | -- | -- | -- |
|  |  |  | 1 |  |  |  |  |
|  | SUJ 4 | -- | -- | -- | -- | -- | -- |
|  | SUJ 5 | -- | -- | -- | -- | -- | -- |